# 적색 발광 액자형 수축

반응·확산 시뮬레이션 물성 · 확보 현황 · 출처

2026-08-06 · MaterialTwin 카탈로그 재료 544종 · 물성값 15,785건 · 출처 1,873건 · 물성 정의 157종

이 문서는 시험계획서(산소영향성 시험계획)가 요구하는 산소 확산 × Stern-Volmer 소광 모델의 입력 물성을 해석 단계별로 정리하고, 확보한 값과 그 출처를 전부 수록한다. 수록된 값은 모두 원문에 인쇄된 수치이며, 그래프에서 읽은 값·역산한 값·문헌 취합표의 재인용은 포함하지 않는다.

# 1. 결론 — 지금 되는 것과 안 되는 것

시험 조건 설계용 프로토타입은 지금 돌릴 수 있다. 설계 판단(목표 수명 역산)은 못 한다.

이 구분은 시험계획이 스스로 정한 순서와 일치한다 — “프로토타입을 시험 착수 전에 완성해 시험 조건 설계에 활용한다.”

지금 되는 것

| 항목 | 근거 |
| --- | --- |
| 가설 검증식 — R/G/B 폭 비율이 τ₀ 비율을 따르는가 | τ₀ 34종 / 73건. 적·녹·청 전부 확보 |
| UV 리셋 기전 판별 — 개시제 계열로 성립/불성립이 갈린다 | 몰흡광계수 6종 / 16건 |
| UV·외광 도달 경로 — 적색 CF의 400 nm 창 | 분광 투과율 실측 확보 |
| 기하 논거 — 왜 4변 대칭 액자인가 | 에지 경로 vs 면방향에 약 9자리 차 |
| 파라미터 스윕 — 시간 법칙 형태, 온도 가속 계수 범위 | 투과도 48종 / 104건, Ea 14종 / 26건 |

지금 안 되는 것

| 못 하는 것 | 없는 물성 |
| --- | --- |
| 절대 시간 스케일 — “3개월이면 액자 폭 몇 mm” | 실제 OCA의 O₂ 확산계수 D · 용해도 S가 0건 |
| R/G/B 절대 소광량 (비율은 가능) | OLED 도판트 계열의 k_q가 0건 |
| 가역 구간의 시한 — 언제부터 회수 불능인가 | 목표 계열의 일중항 산소 수율 Φ_Δ가 0건 |

단서 — D가 없다는 것은 시뮬레이션이 못 돈다는 뜻이 아니다. D는 원래 캘리브레이션 대상이다. 시험계획 Phase 2(온도 3수준 × 시간 5시점)가 w(t) ∝ √(D_eff·t)에서 D_eff를 역피팅하는 설계이고, 문서도 “미지수가 사실상 두 개로 줄고 나머지는 문헌치와 별도 측정으로 고정된다”고 썼다. 시험 전에 절대값을 못 낼 뿐, 모델 골격과 시험 조건 설계는 지금 가능하다.

# 2. 데이터가 시험계획에 대해 말한 것

## 2.1  τ₀ 순서는 R > G > B 가 아니라 R > B > G 다

같은 논문·같은 프로토콜(탈기 CH₂Cl₂) 안에서만 비교한 값이다.

|  | τ₀ | 녹색 대비 |
| --- | --- | --- |
| 녹색 인광 Ir(ppy)₂(acac) | 0.73 µs | 1.00× |
| 청색 인광 FIrpic | 1.82 µs | 2.49× |
| 적색 인광 piq 계열 | 3.90 ~ 11.2 µs | 5.3 ~ 15.3× |
| 청색 형광 (단일지수) pSFIAc1/2 | 7.7 ~ 8.0 ns | — |

적/청 판별력

| 청색 기준 | 배율 |
| --- | --- |
| 청색 인광 FIrpic 1.82 µs | 2.1 ~ 6.2배 |
| 청색 형광 1.6 ~ 13 ns | 300 ~ 7,000배 |
| 순수 형광(단일지수) 7.7 ~ 8.0 ns | 488 ~ 1,455배 |

보고서 문구 확인 — 임원보고의 “적·녹은 발광 지속시간이 청색보다 1000배 가까이 길어”는 청색이 형광일 때 488~1,455배로 정확하다. 다만 이것은 유도된 결과가 아니라 전제다. 청색 인광 스택이면 2~6배로 떨어져 판별력이 거의 사라지므로, 문서에 전제를 명시할 것.

## 2.2  τ₀만으로는 소광량을 예측할 수 없다 — 매질이 그만큼 지배한다

같은 PtOEP를 매질만 바꿔 잰 값이다.

| 매질 | τ₀ (진공) | 공기 중 | 소광비 |
| --- | --- | --- | --- |
| PCL 나노섬유 | 60.5 µs | 6.2 µs | 9.76× |
| PU Tecophilic | 80.8 µs | 11.1 µs | 7.28× |
| PS 나노섬유 | 83.9 µs | 15.2 µs | 5.52× |
| PVDF-HFP | 81.4 µs | 62.0 µs | 1.31× |

τ₀가 80 µs로 거의 같은데 소광비가 7배 갈린다. 시험 판정식에 반영할 것 — Phase 1의 R/G/B 폭 비율이 τ₀ 비율과 어긋나도 곧바로 기각이 아니다. 적·녹·청 발광층의 호스트가 다르면 매질 항이 개입한다.

## 2.3  개시제 계열 하나로 가설이 갈린다

| 계열 | 385~405 nm 몰흡광계수 |
| --- | --- |
| 아실포스핀옥사이드 TPO · BAPO(819) | 51 ~ 66 m²/mol |
| 하이드록시알킬페논 184 · 1173 · 2959 계열 | 0.2 ~ 0.4 m²/mol |

170 ~ 330배 차이다. OCA에 아실포스핀옥사이드계가 들어 있으면 H1c의 UV 리셋 기전이 성립하고, 하이드록시알킬페논계만 있으면 성립하지 않는다. 시험계획 §11의 “OCA 광개시제 계열” 업체 요청이 왜 결정적인지가 이것으로 확정된다 — 공문 회신 하나로 Phase 1 착수 전에 가설을 걸러낼 수 있다.

부수 예측 — TPO 흡수가 395 → 420 nm에서 1/25로 급락한다. 따라서 UV 액션 스펙트럼의 장파장 끝이 415~420 nm에 걸려야 한다. 시험이 이를 확인하면 H1c의 강한 증거다.

## 2.4  적색 CF의 2차 투과창은 실재하고 의도된 것이다

실제 경화막(0.9~1.0 µm) 실측이다.

| 시료 | T400 | T530 (자기 저지대) | T610 (통과대역) |
| --- | --- | --- | --- |
| Example 14 (1.0 µm) | 10 % | 9 % | 99 % |
| Example 23 (1.0 µm) | 17 % | 11 % | 70 % |
| Example 24 (0.9 µm) | 16 % | 11 % | 72 % |

세 시료 모두 T400 > T530 이다 — 잔류 누설이 아니라 별도의 창이다. T410은 다른 특허의 청구항이 0.4 < T410 < 4 를 요구한다. 색도·콘트라스트를 맞추려고 의도적으로 열어 둔 창이지 사고가 아니다. 이 창이 개시제 흡수대(TPO 380 nm 52~57 m²/mol)와 정확히 겹친다.

## 2.5  가교밀도 — 부호가 뒤집히는 계가 있다

가교제 함량 조건이 붙은 산소투과도 53건 / 17재료. 11계 중 9계는 가설 방향이지만 2계가 반대다.

| 계 | 가교제 | P (Barrer) | 방향 |
| --- | --- | --- | --- |
| PEGDA / 2-EEA | 94.7 → 35 wt% | 5.3 → 19 | 가설대로 ↑ |
| BPAEDA4 / PEGMEA | 85 → 28 wt% | 1.6 → 14 | 가설대로 ↑ (8.8배) |
| PEGDA / 2-HEA | 96 → 40 wt% | 4.4 → 0.45 | 반대 ↓ (10배 감소) |
| PEGDA / DEGPEA | 92 → 0 wt% | 4.4 → 2.9 | 반대 ↓ |

하이드록실·페닐 공단량체가 사슬 패킹을 조여 가교밀도 효과를 뒤집는다. 가교밀도만으로 OCA를 외삽하면 안 된다 — 공단량체 화학이 부호를 바꾼다. 비가교(0 wt%) 하한점 2건(2.9 · 7.0 Barrer)을 확보했다. “미경화 OCA가 고속 통로”를 직접 시험할 수 있는 유일한 0점이다.

# 3. 해석 단계별 물성 요구와 확보 현황

## 3.1  산소 확산장 — 에지에서 중앙으로

| 물성 | 단위 | 확보 | 왜 필요한가 |
| --- | --- | --- | --- |
| O₂ 확산계수 D | m²/s | 5종 / 6건 | 액자 폭의 시간 법칙 w(t) ∝ √(D·t)를 정한다 |
| 헨리 용해도 S | mol/(m³·Pa) | 11종 / 16건 | 외기 산소 분압 → 막 내부 용존 농도의 경계조건 c = S·pO₂ |
| 산소 투과도 P | mol/(m·s·Pa) | 72종 / 131건 | P = D·S. 에지 경로와 면방향의 상대 크기를 정한다 |
| 활성화에너지 Ea | J/mol | 14종 / 26건 | 온도 가속 계수 — 시험계획 Phase 2가 온도 3수준을 도는 근거 |

## 3.2  Stern-Volmer 소광

| 물성 | 단위 | 확보 | 왜 필요한가 |
| --- | --- | --- | --- |
| 여기수명 τ₀ | s | 42종 / 95건 | I₀/I = 1 + k_q·τ₀·[O₂]. R/G/B 선택성을 결정하는 핵심 항 |
| Stern-Volmer 상수 K_SV | 1/Pa | 6종 / 6건 | K_SV = k_q·τ₀. 분압에서 소광비를 직접 준다 |
| 소광 속도상수 k_q | m³/(mol·s) | 3종 / 3건 | 소광의 절대 크기. τ₀와 곱해 K_SV가 된다 |
| 광발광 양자수율 PLQY | 1 | 25종 / 42건 | 탈기/공기 쌍이 있으면 산소 소광이 직접 관측된다 |

## 3.3  UV 리셋 — 잔류 개시제 라디칼의 산소 소거

| 물성 | 단위 | 확보 | 왜 필요한가 |
| --- | --- | --- | --- |
| 몰흡광계수 ε | m²/mol | 11종 / 21건 | 개시제 흡수대와 UV 액션 스펙트럼의 겹침 — H1c의 판별 지문 |

## 3.4  UV·외광의 내부 도달 경로

| 물성 | 단위 | 확보 | 왜 필요한가 |
| --- | --- | --- | --- |
| 분광 투과율 T | 1 | 5종 / 78건 | 적색 CF의 380~420 nm 2차 투과창 — 외광이 적색 화소에 닿는 경로 |

## 3.5  비가역 전이 — 가역 구간의 시한

| 물성 | 단위 | 확보 | 왜 필요한가 |
| --- | --- | --- | --- |
| 일중항 산소 수율 Φ_Δ | 1 | 13종 / 13건 | 소광 에너지가 ¹O₂로 넘어가 영구 광산화로 전이하는 비율 |

## 3.6  에지 경로 vs 면방향 — 9자리 차이

1 Barrer = 3.3464e-16 mol·m/(m²·s·Pa)

| 재료 | 산소 투과도 (Barrer) |
| --- | --- |
| TFE ALD Al₂O₃ 38 nm | 6.5e-08 |
| Toppan GX-P-F 배리어필름 | 1.8e-05 |
| Upilex-S | 0.00031 |
| PET | 0.029 |
| Kapton HN | 0.147 |
| PC | 0.745 |
| 아크릴레이트(고무상) 하한 | 19 |

TFE 면방향과 OCA 에지 경로 사이가 약 9자리 벌어진다. “산소는 에지로만 들어온다”는 4변 대칭 논거의 정량 근거가 이것이다.

# 4. 확보한 물성값 전량과 출처

값은 전부 원문에 인쇄된 수치다. tier 1 = 그 재료를 직접 측정해 인쇄한 값, tier 2 = 핸드북·공인 DB, tier 3 = 클래스 대표값·2차 인용, tier 4 = 가정·추정값.

## 4.1  산소 확산장 — 에지에서 중앙으로

### O₂ 확산계수 D  (m²/s)  —  6건

| 재료 | 값 | 등급 | 조건 | 출처 |
| --- | --- | --- | --- | --- |
| PDMS dense membrane (polydimethylsiloxane, gas trans | 3.1e-09 | t1 | species=O2, temperature_K=293, pressure_Pa=101300, test_method=lag-time method, residual gas analyzer (RGA), m… | [1] |
| PMMA Optical (Acrylic) | 2.49e-12 | t3 | species=O2, temperature_C=25 | [2] |
| PMMA Optical (Acrylic) | 1.9e-12 | t3 | species=O2, state=glassy PMMA film, value_basis=리뷰 본문이 인용한 2차 값 — 원논문(Klinger 2009) 미확인, 온도 미기재 | [3] |
| PTFE (RF coax dielectric) | 1.36e-12 | t2 | species=O2, temperature_C=25 | [2] |
| Prism Sheet / BEF (PET) | 2.7e-13 | t3 | species=O2, temperature_C=25 | [2] |
| Sylgard 184 (PDMS, Dow) | 3.1e-09 | t3 | species=O2, temperature_K=293, grade_scope=class value, test_method=lag-time method (RGA) | [1] |

출처

| # | 제목 | DOI / URL | 종류 |
| --- | --- | --- | --- |
| [1] | The Role of Surfaces in Gas Transport Through Polymer Membranes | DOI 10.3390/polym11050910 | journal |
| [2] | Water Vapor Permeation in Plastics (PNNL-26070), Table 4.3 — Some Water Vapor Permeability Coefficients [Bhadha 1999] | https://www.pnnl.gov/main/publications/external/technical_reports/PNNL-26070.pdf | other |
| [3] | Organic Polymer Hosts for Triplet-Triplet Annihilation Upconversion Systems (Macromolecules 2021, 54, 5, 2255-2270) — 본문이 Mogri Z.; Paul D. R. Polymer | DOI 10.1021/acs.macromol.1c00133 | journal |

### 헨리 용해도 S  (mol/(m³·Pa))  —  16건

| 재료 | 값 | 등급 | 조건 | 출처 |
| --- | --- | --- | --- | --- |
| ARclear 42010 optically clear silicone adhesive tran | 9e-05 | t3 | species=O2, temperature_K=293, pressure_Pa=101300, grade_scope=class value — 순수 PDMS 치밀막(두께 2 mm) 측정값이다. 이 재료는… | [1] |
| ARclear 43080 optically clear high-peel silicone adh | 9e-05 | t3 | species=O2, temperature_K=293, pressure_Pa=101300, grade_scope=class value — 순수 PDMS 치밀막(두께 2 mm) 측정값이다. 이 재료는… | [1] |
| ARclear 8932EE optically clear silicone adhesive tra | 9e-05 | t3 | species=O2, temperature_K=293, pressure_Pa=101300, grade_scope=class value — 순수 PDMS 치밀막(두께 2 mm) 측정값이다. 이 재료는… | [1] |
| ARclear 93495 optically clear silicone adhesive tran | 9e-05 | t3 | species=O2, temperature_K=293, pressure_Pa=101300, grade_scope=class value — 순수 PDMS 치밀막(두께 2 mm) 측정값이다. 이 재료는… | [1] |
| E-44 (WSR6101) bisphenol-A epoxy potting resin, Jeff | 9.44e-05 | t3 | species=O2, temperature_C=25, thickness_um=150, humidity_rh=0, grade_scope=class value — 원 시료는 Epon 828(DGEBA)… | [2] |
| E-44 (WSR6101) bisphenol-A epoxy potting resin, Jeff | 7.63e-05 | t3 | species=O2, temperature_C=40, thickness_um=150, humidity_rh=0, grade_scope=class value — 원 시료는 Epon 828(DGEBA)… | [2] |
| E-44 (WSR6101) bisphenol-A epoxy potting resin, Jeff | 5.19e-05 | t3 | species=O2, temperature_C=65, thickness_um=150, humidity_rh=0, grade_scope=class value — 원 시료는 Epon 828(DGEBA)… | [2] |
| E-44 (WSR6101) bisphenol-A epoxy potting resin, Jeff | 4.82e-05 | t3 | species=O2, temperature_C=80, thickness_um=150, humidity_rh=0, grade_scope=class value — 원 시료는 Epon 828(DGEBA)… | [2] |
| Epoxy molding resin for power module encapsulation ( | 9.44e-05 | t3 | species=O2, temperature_C=25, humidity_rh=0, grade_scope=class value — 무충전 DGEBA/아민 에폭시(Epon 828/A2049) 값이다. 이… | [2] |
| PDMS dense membrane (polydimethylsiloxane, gas trans | 9e-05 | t2 | species=O2, temperature_K=293, pressure_Pa=101300 | [1] |
| PSA Silicone High-Temp | 9e-05 | t3 | species=O2, temperature_K=293, pressure_Pa=101300, grade_scope=class value — 순수 PDMS 치밀막(두께 2 mm) 측정값이다. 이 재료는… | [1] |
| Polyimide gas separation membrane (UBE UMS-A2 module | 0.0001337 | t2 | species=O2, temperature_K=308, sorption_region=Henry region only (dual-mode sorption k_D; Langmuir 성분 제외) | [3] |
| Polyimide gas separation membrane (UBE UMS-A2 module | 0.0001186 | t2 | species=O2, temperature_K=318, sorption_region=Henry region only (dual-mode sorption k_D; Langmuir 성분 제외) | [3] |
| Polyimide gas separation membrane (UBE UMS-A2 module | 0.0001059 | t2 | species=O2, temperature_K=328, sorption_region=Henry region only (dual-mode sorption k_D; Langmuir 성분 제외) | [3] |
| Silicone OCA (Momentive, MQ resin / silicone gum) | 9e-05 | t3 | species=O2, temperature_K=293, pressure_Pa=101300, grade_scope=class value — 순수 PDMS 치밀막(두께 2 mm) 측정값이다. 이 재료는… | [1] |
| Sylgard 184 (PDMS, Dow) | 9e-05 | t3 | species=O2, temperature_K=293, grade_scope=class value | [1] |

출처

| # | 제목 | DOI / URL | 종류 |
| --- | --- | --- | --- |
| [1] | The Role of Surfaces in Gas Transport Through Polymer Membranes | DOI 10.3390/polym11050910 | journal |
| [2] | A Critical Review of the Time-Dependent Performance of Polymeric Pipeline Coatings: Focus on Hydration of Epoxy-Based Coatings — Table 3, Oxygen mass | DOI 10.3390/polym13091517 | journal |
| [3] | Transport of Carbon Dioxide, Methane, Oxygen and Nitrogen in a Glassy Polyimide Membrane | DOI 10.3390/molecules30234524 | journal |

### 산소 투과도 P  (mol/(m·s·Pa))  —  131건

| 재료 | 값 | 등급 | 조건 | 출처 |
| --- | --- | --- | --- | --- |
| 3M Foldable OCA CEF3501 | 35.3 Barrer | t3 | species=O2, temperature_C=35, state=amorphous (P35+), pressure_atm_upstream=2, value_basis=Arrhenius 외삽값 — 35 … | [1] |
| 3M Optically Clear Adhesive 8172 | 35.3 Barrer | t3 | species=O2, temperature_C=35, state=amorphous (P35+), pressure_atm_upstream=2, value_basis=Arrhenius 외삽값 — 35 … | [1] |
| 3M Optically Clear Adhesive 8211 | 35.3 Barrer | t3 | species=O2, temperature_C=35, state=amorphous (P35+), pressure_atm_upstream=2, value_basis=Arrhenius 외삽값 — 35 … | [1] |
| ARclear 42010 optically clear silicone adhesive tran | 836.7 Barrer | t3 | species=O2, temperature_K=293, pressure_Pa=101300, grade_scope=class value — 순수 PDMS 치밀막(두께 2 mm) 측정값이다. 이 재료는… | [2] |
| ARclear 43080 optically clear high-peel silicone adh | 836.7 Barrer | t3 | species=O2, temperature_K=293, pressure_Pa=101300, grade_scope=class value — 순수 PDMS 치밀막(두께 2 mm) 측정값이다. 이 재료는… | [2] |
| ARclear 8932EE optically clear silicone adhesive tra | 836.7 Barrer | t3 | species=O2, temperature_K=293, pressure_Pa=101300, grade_scope=class value — 순수 PDMS 치밀막(두께 2 mm) 측정값이다. 이 재료는… | [2] |
| ARclear 93495 optically clear silicone adhesive tran | 836.7 Barrer | t3 | species=O2, temperature_K=293, pressure_Pa=101300, grade_scope=class value — 순수 PDMS 치밀막(두께 2 mm) 측정값이다. 이 재료는… | [2] |
| Comfi Daily disposable contact lens (etafilcon A, HE | 17.4 Barrer | t1 | species=O2, state=hydrated (PBS 침지 후), test_method=ISO 18369-4:2017 polarographic (Rehder 곡면셀 + Createch 201T) | [3] |
| E-44 (WSR6101) bisphenol-A epoxy potting resin, Jeff | 0.1404 Barrer | t3 | species=O2, temperature_C=25, thickness_um=150, humidity_rh=0, grade_scope=class value — 원 시료는 Epon 828(DGEBA)… | [4] |
| E-44 (WSR6101) bisphenol-A epoxy potting resin, Jeff | 0.2391 Barrer | t3 | species=O2, temperature_C=40, thickness_um=150, humidity_rh=0, grade_scope=class value — 원 시료는 Epon 828(DGEBA)… | [4] |
| E-44 (WSR6101) bisphenol-A epoxy potting resin, Jeff | 0.508 Barrer | t3 | species=O2, temperature_C=65, thickness_um=150, humidity_rh=0, grade_scope=class value — 원 시료는 Epon 828(DGEBA)… | [4] |
| E-44 (WSR6101) bisphenol-A epoxy potting resin, Jeff | 0.768 Barrer | t3 | species=O2, temperature_C=80, thickness_um=150, humidity_rh=0, grade_scope=class value — 원 시료는 Epon 828(DGEBA)… | [4] |
| Epoxy molding resin for power module encapsulation ( | 0.1404 Barrer | t3 | species=O2, temperature_C=25, humidity_rh=0, grade_scope=class value — 무충전 DGEBA/아민 에폭시(Epon 828/A2049) 값이다. 이… | [4] |
| HD MicroSystems PI-2525 polyimide (PMDA/ODA, spin-co | 0.1279 Barrer | t3 | temperature_C=23, thickness_um=75, relative_humidity_pct=0, test_standard=ASTM D3985 (Mocon OX-TRAN 2/21 ML), … | [5] |
| Lexan 8010MC polycarbonate film (100 um, ALD barrier | 0.7452 Barrer | t1 | species=O2, temperature_C=23, thickness_um=100, humidity_rh=0, test_instrument=Labthink C130 gas permeability … | [6] |
| Non-silicone hydrogel CL, Sample 3E-B (DMAA 79.64 / | 73.9 Barrer | t1 | species=O2, crosslinker_wt_pct=0.27, state=hydrated, 함수율 80.28%, crosslinker=tri(ethylene glycol) dimethacryla… | [3] |
| OCA 8211 (3M, rigid standard) | 35.3 Barrer | t3 | species=O2, temperature_C=35, state=amorphous (P35+), pressure_atm_upstream=2, value_basis=Arrhenius 외삽값 — 35 … | [1] |
| OCA Foldable (Tg<-30C) | 35.3 Barrer | t3 | species=O2, temperature_C=35, state=amorphous (P35+), pressure_atm_upstream=2, value_basis=Arrhenius 외삽값 — 35 … | [1] |
| OCA Rigid High Bond | 35.3 Barrer | t3 | species=O2, temperature_C=35, state=amorphous (P35+), pressure_atm_upstream=2, value_basis=Arrhenius 외삽값 — 35 … | [1] |
| OCA Rigid Standard (3M 8171) | 35.3 Barrer | t3 | species=O2, temperature_C=35, state=amorphous (P35+), pressure_atm_upstream=2, value_basis=Arrhenius 외삽값 — 35 … | [1] |
| OCA Rollable (Tg<-40C) | 35.3 Barrer | t3 | species=O2, temperature_C=35, state=amorphous (P35+), pressure_atm_upstream=2, value_basis=Arrhenius 외삽값 — 35 … | [1] |
| OCA UV Cured | 35.3 Barrer | t3 | species=O2, temperature_C=35, state=amorphous (P35+), pressure_atm_upstream=2, value_basis=Arrhenius 외삽값 — 35 … | [1] |
| OCA acrylic (flexible device, Tg 0C) - Micromachines | 35.3 Barrer | t3 | species=O2, temperature_C=35, state=amorphous (P35+), pressure_atm_upstream=2, value_basis=Arrhenius 외삽값 — 35 … | [1] |
| OCA acrylic (foldable OLED) - Microsyst Nanoeng 2026 | 35.3 Barrer | t3 | species=O2, temperature_C=35, state=amorphous (P35+), pressure_atm_upstream=2, value_basis=Arrhenius 외삽값 — 35 … | [1] |
| PDMS crosslinked membrane (TEOS 가교제 0-30 wt% 시리즈, Ra | 640 Barrer | t3 | species=O2, crosslinker_teos_wt_pct=0, pressure_bar=0.5, temperature=미상 — 인용 문장에 미기재 | [7] |
| PDMS crosslinked membrane (TEOS 가교제 0-30 wt% 시리즈, Ra | 185 Barrer | t3 | species=O2, crosslinker_teos_wt_pct=30, pressure_bar=0.5, temperature=미상 — 인용 문장에 미기재 | [7] |
| PDMS dense membrane (polydimethylsiloxane, gas trans | 836.7 Barrer | t1 | species=O2, temperature_K=293, pressure_Pa=101300, test_method=variable pressure / high-vacuum chamber, membra… | [2] |
| PE packaging film (45 um, uncoated barrier reference | 0.4797 Barrer | t3 | species=O2, thickness_um=45, temperature=미상 — 논문이 시험 온도·습도를 미기재, test_instrument=Systech Illinois 8001 Oxygen … | [8] |
| PECVD SiOx barrier film, 150 nm SiOx on 45 um PE (HM | 0.03754 Barrer | t3 | species=O2, thickness_um=45.15, coating_thickness_nm=150, deposition=PECVD, surface_pretreatment=Ar + ethanol … | [8] |
| PECVD SiOx barrier film, 150 nm SiOx on 45 um PE (HM | 0.05095 Barrer | t3 | species=O2, thickness_um=45.15, coating_thickness_nm=150, deposition=PECVD, surface_pretreatment=Ar + allylami… | [8] |
| PECVD SiOx barrier film, 150 nm SiOx on 45 um PE (HM | 0.05817 Barrer | t3 | species=O2, thickness_um=45.15, coating_thickness_nm=150, deposition=PECVD, surface_pretreatment=Ar + acrylic … | [8] |
| PEN Film (Diaphragm) | 0.007615 Barrer | t2 | temperature_C=25, pressure_atm=1 | [9] |
| PI Base Film — Kapton HN (DuPont) | 0.1466 Barrer | t1 | temperature_C=23, thickness_um=25, relative_humidity_pct=50, test_method=ASTM D-1434 (1988) | [10] |
| PI Base Film — Kapton HN (DuPont) | 0.1467 Barrer | t1 | temperature_C=23, thickness_um=25, relative_humidity_pct=50, test_standard=ASTM D-1434-82 | [11] |
| PI Base Film — Upilex-25RN (UBE) | 0.03858 Barrer | t1 | temperature_C=30, thickness_um=25, pressure_bar=1.0, test_standard=ASTM D1434 | [12] |
| PI Base Film — Upilex-S (UBE) | 0.0003086 Barrer | t1 | temperature_C=30.0, thickness_um=25.0, pressure_bar=1.0, test_method=ASTM D1434 | [13] |
| PMMA Optical (Acrylic) | 0.08833 Barrer | t3 | temperature_C=25, pressure_atm=1 | [9] |
| PMMA Optical (Acrylic) | 0.1431 Barrer | t3 | species=O2, temperature_C=25, humidity_rh=0, pressure_atm=1, grade_scope=class value | [14] |
| PMMA Optical (Acrylic) | 0.127 Barrer | t3 | species=O2, temperature_C=25, humidity_rh=50, pressure_atm=1, grade_scope=class value | [14] |
| PMMA Optical (Acrylic) | 0.1201 Barrer | t3 | species=O2, temperature_C=25, humidity_rh=80, pressure_atm=1, grade_scope=class value | [14] |
| PSA Acrylic General (3M 467MP) | 35.3 Barrer | t3 | species=O2, temperature_C=35, state=amorphous (P35+), pressure_atm_upstream=2, value_basis=Arrhenius 외삽값 — 35 … | [1] |
| PSA High Shear (Nitto 5000) | 35.3 Barrer | t3 | species=O2, temperature_C=35, state=amorphous (P35+), pressure_atm_upstream=2, value_basis=Arrhenius 외삽값 — 35 … | [1] |
| PSA Removable | 35.3 Barrer | t3 | species=O2, temperature_C=35, state=amorphous (P35+), pressure_atm_upstream=2, value_basis=Arrhenius 외삽값 — 35 … | [1] |
| PSA Rubber Hot-Melt (SIS/C5 tackifier, 20um on 50um | 23.4 Barrer | t3 | species=O2, temperature_C=25, grade_scope=class value — 순수 poly(isoprene) 값이다. 이 재료는 SIS 블록공중합체 + C5 탄화수소 점착부여… | [15] |
| PSA Silicone High-Temp | 836.7 Barrer | t3 | species=O2, temperature_K=293, pressure_Pa=101300, grade_scope=class value — 순수 PDMS 치밀막(두께 2 mm) 측정값이다. 이 재료는… | [2] |
| PVDF Binder | 0.08406 Barrer | t3 | temperature_C=25, pressure_atm=1 | [9] |
| Parylene Conformal Coating | 0.04264 Barrer | t1 | temperature_C=25, grade=Parylene C, test_method=ASTM D1434 | [16] |
| Parylene Conformal Coating | 0.04266 Barrer | t1 | temperature_C=25, test_standard=ASTM D1434, parylene_type=C | [16] |
| Parylene HT Conformal Coating | 0.358 Barrer | t1 | temperature_C=25, grade=Parylene HT, test_method=MOCON MULTI-TRAN 400 | [16] |
| Parylene HT Conformal Coating | 0.3581 Barrer | t1 | temperature_C=25, test_method=MOCON MULTI-TRAN 400 | [16] |
| Poly(decyl acrylate) (PA 10, n-alkyl acrylate homopo | 31.1 Barrer | t3 | species=O2, temperature_C=35, state=amorphous / molten (P35+), pressure_atm_upstream=2, value_basis=Arrhenius … | [1] |
| Poly(docosyl acrylate) (PA 22, n-alkyl acrylate homo | 92.1 Barrer | t3 | species=O2, temperature_C=35, state=molten / amorphous (P35+, Tm 위), pressure_atm_upstream=2, side_chain_carbo… | [1] |
| Poly(docosyl acrylate) (PA 22, n-alkyl acrylate homo | 1 Barrer | t3 | species=O2, temperature_C=35, state=semi-crystalline (P35-, Tm 아래 결정상), pressure_atm_upstream=2, side_chain_ca… | [1] |
| Poly(docosyl acrylate) (PA 22, n-alkyl acrylate homo | 76.3 Barrer | t3 | species=O2, side_chain_carbons=22, value_basis=리뷰 본문이 인용한 2차 값 — 원표(Mogri & Paul 2001) 미확인, 결정/융해 상태 미기재 | [17] |
| Poly(dodecyl acrylate) (PA 12, n-alkyl acrylate homo | 52 Barrer | t3 | species=O2, temperature_C=35, state=molten / amorphous (P35+, Tm 위), pressure_atm_upstream=2, side_chain_carbo… | [1] |
| Poly(dodecyl acrylate) (PA 12, n-alkyl acrylate homo | 42 Barrer | t3 | species=O2, temperature_C=35, state=semi-crystalline (P35-, Tm 아래 결정상), pressure_atm_upstream=2, side_chain_ca… | [1] |
| Poly(ethyl acrylate) (PEA, n-alkyl acrylate homopoly | 19 Barrer | t3 | species=O2, side_chain_carbons=2, value_basis=리뷰 본문이 인용한 2차 값 — 원표(Mogri & Paul 2001) 미확인 | [17] |
| Poly(hexyl acrylate) (PA 6, n-alkyl acrylate homopol | 35.3 Barrer | t3 | species=O2, temperature_C=35, state=amorphous / molten (P35+), pressure_atm_upstream=2, value_basis=Arrhenius … | [1] |
| Poly(methyl acrylate) (PMA, n-alkyl acrylate homopol | 1.06 Barrer | t3 | species=O2, side_chain_carbons=1, value_basis=리뷰 본문이 인용한 2차 값 — 원표(Mogri & Paul 2001) 미확인 | [17] |
| Poly(octadecyl acrylate) (PA 18, n-alkyl acrylate ho | 75 Barrer | t3 | species=O2, temperature_C=35, state=molten / amorphous (P35+, Tm 위), pressure_atm_upstream=2, side_chain_carbo… | [1] |
| Poly(octadecyl acrylate) (PA 18, n-alkyl acrylate ho | 1.2 Barrer | t3 | species=O2, temperature_C=35, state=semi-crystalline (P35-, Tm 아래 결정상), pressure_atm_upstream=2, side_chain_ca… | [1] |
| Poly(tetradecyl acrylate) (PA 14, n-alkyl acrylate h | 56.5 Barrer | t3 | species=O2, temperature_C=35, state=molten / amorphous (P35+, Tm 위), pressure_atm_upstream=2, side_chain_carbo… | [1] |
| Poly(tetradecyl acrylate) (PA 14, n-alkyl acrylate h | 6.6 Barrer | t3 | species=O2, temperature_C=35, state=semi-crystalline (P35-, Tm 아래 결정상), pressure_atm_upstream=2, side_chain_ca… | [1] |
| Prism Sheet / BEF (PET) | 0.02894 Barrer | t3 | temperature_C=25, thickness_um=100, pressure_atm=1, test_standard=ASTM D1434-72 | [18] |
| Silane-modified acrylic hydrogel CL, 2T20 (2TSEMA 16 | 30.53 Barrer | t1 | species=O2, crosslinker_wt_pct=0.82, state=hydrated (수화 상태), crosslinker=ethylene glycol dimethacrylate (EGDMA… | [19] |
| Silane-modified acrylic hydrogel CL, 2TT1 (2TSEMA 16 | 39.52 Barrer | t1 | species=O2, crosslinker_wt_pct=0.82, state=hydrated (수화 상태), crosslinker=ethylene glycol dimethacrylate (EGDMA… | [19] |
| Silane-modified acrylic hydrogel CL, Ref (Sil-OH 32. | 25.79 Barrer | t1 | species=O2, crosslinker_wt_pct=0.99, state=hydrated (수화 상태), crosslinker=ethylene glycol dimethacrylate (EGDMA… | [19] |
| Silicone OCA (Momentive, MQ resin / silicone gum) | 836.7 Barrer | t3 | species=O2, temperature_K=293, pressure_Pa=101300, grade_scope=class value — 순수 PDMS 치밀막(두께 2 mm) 측정값이다. 이 재료는… | [2] |
| Thin-Film Encapsulation (Al2O3) | 6.465e-08 Barrer | t3 | species=O2, temperature_C=23, humidity_rh=0, thickness_nm=38.09, deposition=PEALD, substrate=polycarbonate fil… | [6] |
| Toppan GL-AE transparent barrier film (AlOx-coated P | 9.137e-05 Barrer | t1 | species=O2, temperature_C=30, thickness_um=12, humidity_rh=70, deposition=vacuum-deposited AlOx on PET, standa… | [20] |
| Toppan GL-AEC-F transparent barrier film (AlOx-coate | 5.482e-05 Barrer | t1 | species=O2, temperature_C=30, thickness_um=12, humidity_rh=70, deposition=vacuum-deposited AlOx on PET, standa… | [21] |
| Toppan GL-ARH transparent barrier film (AlOx-coated | 5.482e-05 Barrer | t1 | species=O2, temperature_C=30, thickness_um=12, humidity_rh=70, deposition=vacuum-deposited AlOx on PET, standa… | [22] |
| Toppan GL-BP-F transparent barrier film (SiOx-coated | 5.482e-05 Barrer | t1 | species=O2, temperature_C=30, thickness_um=18, humidity_rh=70, deposition=vacuum-deposited SiOx on PP, standar… | [23] |
| Toppan GL-RD transparent barrier film (SiOx-coated P | 3.655e-05 Barrer | t1 | species=O2, temperature_C=30, thickness_um=12, humidity_rh=70, deposition=vacuum-deposited SiOx on PET, standa… | [24] |
| Toppan GX-P-F transparent barrier film (AlOx-coated | 1.827e-05 Barrer | t1 | species=O2, temperature_C=30, thickness_um=12, humidity_rh=70, deposition=vacuum-deposited AlOx on PET, standa… | [25] |
| UV-cured BPAEDA15 homopolymer acrylate network (가교제 | 7.3 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (UV 광경화, 수추출 후 건조), crosslinker_wt_pct=100, crosslinker=b… | [26] |
| UV-cured BPAEDA15/DEGEEA acrylate network (BPAEDA15 | 11 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (UV 광경화, 수추출 후 건조), crosslinker_wt_pct=80, crosslinker=bi… | [26] |
| UV-cured BPAEDA15/DEGEEA acrylate network (BPAEDA15 | 12 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (UV 광경화, 수추출 후 건조), crosslinker_wt_pct=70, crosslinker=bi… | [26] |
| UV-cured BPAEDA15/DEGEEA acrylate network (BPAEDA15 | 14 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (UV 광경화, 수추출 후 건조), crosslinker_wt_pct=60, crosslinker=bi… | [26] |
| UV-cured BPAEDA15/DEGEEA acrylate network (BPAEDA15 | 15 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (UV 광경화, 수추출 후 건조), crosslinker_wt_pct=50, crosslinker=bi… | [26] |
| UV-cured BPAEDA15/PEGMEA acrylate network (BPAEDA15 | 9.3 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (UV 광경화, 수추출 후 건조), crosslinker_wt_pct=80, crosslinker=bi… | [26] |
| UV-cured BPAEDA15/PEGMEA acrylate network (BPAEDA15 | 11 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (UV 광경화, 수추출 후 건조), crosslinker_wt_pct=70, crosslinker=bi… | [26] |
| UV-cured BPAEDA15/PEGMEA acrylate network (BPAEDA15 | 12 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (UV 광경화, 수추출 후 건조), crosslinker_wt_pct=60, crosslinker=bi… | [26] |
| UV-cured BPAEDA15/PEGMEA acrylate network (BPAEDA15 | 15 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (UV 광경화, 수추출 후 건조), crosslinker_wt_pct=50, crosslinker=bi… | [26] |
| UV-cured BPAEDA4 homopolymer acrylate network (가교제 1 | 0.9 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (UV 광경화, 수추출 후 건조), crosslinker_wt_pct=100, crosslinker=b… | [26] |
| UV-cured BPAEDA4/PEGA acrylate network (BPAEDA4 가교제 | 1 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (UV 광경화, 수추출 후 건조), crosslinker_wt_pct=88, crosslinker=bi… | [26] |
| UV-cured BPAEDA4/PEGA acrylate network (BPAEDA4 가교제 | 1.9 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (UV 광경화, 수추출 후 건조), crosslinker_wt_pct=73, crosslinker=bi… | [26] |
| UV-cured BPAEDA4/PEGA acrylate network (BPAEDA4 가교제 | 2.1 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (UV 광경화, 수추출 후 건조), crosslinker_wt_pct=55, crosslinker=bi… | [26] |
| UV-cured BPAEDA4/PEGA acrylate network (BPAEDA4 가교제 | 3.5 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (UV 광경화, 수추출 후 건조), crosslinker_wt_pct=31, crosslinker=bi… | [26] |
| UV-cured BPAEDA4/PEGMEA acrylate network (BPAEDA4 가교 | 1.6 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (UV 광경화, 수추출 후 건조), crosslinker_wt_pct=85, crosslinker=bi… | [26] |
| UV-cured BPAEDA4/PEGMEA acrylate network (BPAEDA4 가교 | 3.2 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (UV 광경화, 수추출 후 건조), crosslinker_wt_pct=70, crosslinker=bi… | [26] |
| UV-cured BPAEDA4/PEGMEA acrylate network (BPAEDA4 가교 | 7.5 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (UV 광경화, 수추출 후 건조), crosslinker_wt_pct=50, crosslinker=bi… | [26] |
| UV-cured BPAEDA4/PEGMEA acrylate network (BPAEDA4 가교 | 14 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (UV 광경화, 수추출 후 건조), crosslinker_wt_pct=28, crosslinker=bi… | [26] |
| UV-cured PEGDA/2-EEA acrylate network (PEGDA 가교제 35- | 5.3 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출로 sol 제거 후 건조), crosslinker_wt_pct=94.7… | [26] |
| UV-cured PEGDA/2-EEA acrylate network (PEGDA 가교제 35- | 6.6 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출로 sol 제거 후 건조), crosslinker_wt_pct=88.0… | [26] |
| UV-cured PEGDA/2-EEA acrylate network (PEGDA 가교제 35- | 8.2 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출로 sol 제거 후 건조), crosslinker_wt_pct=76.5… | [26] |
| UV-cured PEGDA/2-EEA acrylate network (PEGDA 가교제 35- | 12 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출로 sol 제거 후 건조), crosslinker_wt_pct=54.8… | [26] |
| UV-cured PEGDA/2-EEA acrylate network (PEGDA 가교제 35- | 19 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출로 sol 제거 후 건조), crosslinker_wt_pct=35.0… | [26] |
| UV-cured PEGDA/2-HEA acrylate network (PEGDA 가교제 40- | 4.4 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출로 sol 제거 후 건조), crosslinker_wt_pct=96.0… | [26] |
| UV-cured PEGDA/2-HEA acrylate network (PEGDA 가교제 40- | 4.6 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출로 sol 제거 후 건조), crosslinker_wt_pct=89.9… | [26] |
| UV-cured PEGDA/2-HEA acrylate network (PEGDA 가교제 40- | 2.4 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출로 sol 제거 후 건조), crosslinker_wt_pct=79.9… | [26] |
| UV-cured PEGDA/2-HEA acrylate network (PEGDA 가교제 40- | 1.1 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출로 sol 제거 후 건조), crosslinker_wt_pct=59.9… | [26] |
| UV-cured PEGDA/2-HEA acrylate network (PEGDA 가교제 40- | 0.45 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출로 sol 제거 후 건조), crosslinker_wt_pct=40.3… | [26] |
| UV-cured PEGDA/DEGEEA acrylate network (PEGDA 가교제 29 | 5.9 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출 후 건조), crosslinker_wt_pct=94, crosslin… | [26] |
| UV-cured PEGDA/DEGEEA acrylate network (PEGDA 가교제 29 | 7.4 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출 후 건조), crosslinker_wt_pct=85, crosslin… | [26] |
| UV-cured PEGDA/DEGEEA acrylate network (PEGDA 가교제 29 | 9.3 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출 후 건조), crosslinker_wt_pct=71, crosslin… | [26] |
| UV-cured PEGDA/DEGEEA acrylate network (PEGDA 가교제 29 | 14 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출 후 건조), crosslinker_wt_pct=48, crosslin… | [26] |
| UV-cured PEGDA/DEGEEA acrylate network (PEGDA 가교제 29 | 19 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출 후 건조), crosslinker_wt_pct=29, crosslin… | [26] |
| UV-cured PEGDA/DEGPEA acrylate network (PEGDA 가교제 0- | 4.4 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출 후 건조), crosslinker_wt_pct=92, crosslin… | [26] |
| UV-cured PEGDA/DEGPEA acrylate network (PEGDA 가교제 0- | 4.2 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출 후 건조), crosslinker_wt_pct=67, crosslin… | [26] |
| UV-cured PEGDA/DEGPEA acrylate network (PEGDA 가교제 0- | 4 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출 후 건조), crosslinker_wt_pct=43, crosslin… | [26] |
| UV-cured PEGDA/DEGPEA acrylate network (PEGDA 가교제 0- | 3.7 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출 후 건조), crosslinker_wt_pct=25, crosslin… | [26] |
| UV-cured PEGDA/DEGPEA acrylate network (PEGDA 가교제 0- | 2.9 Barrer | t3 | species=O2, temperature_C=35, cure_state=가교제 0 wt% — 단관능 아크릴레이트만 UV 중합한 비가교(선형) 필름, crosslinker_wt_pct=0, cros… | [26] |
| UV-cured PEGDA/EGMEA acrylate network (PEGDA 가교제 37- | 5.5 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출로 sol 제거 후 건조), crosslinker_wt_pct=95.5… | [26] |
| UV-cured PEGDA/EGMEA acrylate network (PEGDA 가교제 37- | 5.2 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출로 sol 제거 후 건조), crosslinker_wt_pct=88.8… | [26] |
| UV-cured PEGDA/EGMEA acrylate network (PEGDA 가교제 37- | 6.7 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출로 sol 제거 후 건조), crosslinker_wt_pct=78.8… | [26] |
| UV-cured PEGDA/EGMEA acrylate network (PEGDA 가교제 37- | 7.3 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출로 sol 제거 후 건조), crosslinker_wt_pct=57.4… | [26] |
| UV-cured PEGDA/EGMEA acrylate network (PEGDA 가교제 37- | 9.2 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출로 sol 제거 후 건조), crosslinker_wt_pct=37.7… | [26] |
| UV-cured PEGDA/PEGPEA acrylate network (PEGDA 가교제 0- | 5.2 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출 후 건조), crosslinker_wt_pct=90, crosslin… | [26] |
| UV-cured PEGDA/PEGPEA acrylate network (PEGDA 가교제 0- | 5.7 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출 후 건조), crosslinker_wt_pct=77, crosslin… | [26] |
| UV-cured PEGDA/PEGPEA acrylate network (PEGDA 가교제 0- | 5.3 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출 후 건조), crosslinker_wt_pct=59, crosslin… | [26] |
| UV-cured PEGDA/PEGPEA acrylate network (PEGDA 가교제 0- | 5.4 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured (312 nm UV, 5일 수추출 후 건조), crosslinker_wt_pct=35, crosslin… | [26] |
| UV-cured PEGDA/PEGPEA acrylate network (PEGDA 가교제 0- | 7 Barrer | t3 | species=O2, temperature_C=35, cure_state=가교제 0 wt% — 단관능 아크릴레이트만 UV 중합한 비가교(선형) 필름, crosslinker_wt_pct=0, cros… | [26] |
| UV-cured PEGDA/TRIS-A acrylate network (PEGDA 가교제 20 | 6.7 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured, crosslinker_pegda_wt_pct=100, crosslinker_pegda_vol_pct=… | [26] |
| UV-cured PEGDA/TRIS-A acrylate network (PEGDA 가교제 20 | 16 Barrer | t1 | species=O2, temperature_C=35, cure_state=fully cured, crosslinker_pegda_wt_pct=80, crosslinker_pegda_vol_pct=7… | [26] |
| UV-cured PEGDA/TRIS-A acrylate network (PEGDA 가교제 20 | 24 Barrer | t1 | species=O2, temperature_C=35, cure_state=fully cured, crosslinker_pegda_wt_pct=70, crosslinker_pegda_vol_pct=6… | [26] |
| UV-cured PEGDA/TRIS-A acrylate network (PEGDA 가교제 20 | 42 Barrer | t1 | species=O2, temperature_C=35, cure_state=fully cured, crosslinker_pegda_wt_pct=60, crosslinker_pegda_vol_pct=5… | [26] |
| UV-cured PEGDA/TRIS-A acrylate network (PEGDA 가교제 20 | 58 Barrer | t1 | species=O2, temperature_C=35, cure_state=fully cured, crosslinker_pegda_wt_pct=50, crosslinker_pegda_vol_pct=4… | [26] |
| UV-cured PEGDA/TRIS-A acrylate network (PEGDA 가교제 20 | 78 Barrer | t1 | species=O2, temperature_C=35, cure_state=fully cured, crosslinker_pegda_wt_pct=40, crosslinker_pegda_vol_pct=3… | [26] |
| UV-cured PEGDA/TRIS-A acrylate network (PEGDA 가교제 20 | 140 Barrer | t1 | species=O2, temperature_C=35, cure_state=fully cured, crosslinker_pegda_wt_pct=20, crosslinker_pegda_vol_pct=1… | [26] |
| UV-cured XLPEGDA-100 network (PEGDA n=14 단독 광경화, 희석 | 5.1 Barrer | t3 | species=O2, temperature_C=35, cure_state=fully cured, 희석 용매 없음, crosslinker_wt_pct=100, crosslinker=PEGDA (pol… | [26] |

출처

| # | 제목 | DOI / URL | 종류 |
| --- | --- | --- | --- |
| [1] | Physical Properties of Poly (n-alkyl acrylate) Copolymers (K. A. O'Leary, PhD dissertation, The University of Texas at Austin, 2005; supervisor D. R. | https://repositories.lib.utexas.edu/server/api/core/bitstreams/b50f3cf2-2ce3-4e44-aba8-a120bd4e0003/content | other |
| [2] | The Role of Surfaces in Gas Transport Through Polymer Membranes | DOI 10.3390/polym11050910 | journal |
| [3] | Optimization of the Oxygen Permeability of Non-Silicone Hydrogel Contact Lenses Through Crosslinking Modifications (Gels 2024, 10, 726) | DOI 10.3390/gels10110726 | journal |
| [4] | A Critical Review of the Time-Dependent Performance of Polymeric Pipeline Coatings: Focus on Hydration of Epoxy-Based Coatings — Table 3, Oxygen mass | DOI 10.3390/polym13091517 | journal |
| [5] | Zhang et al., High-Barrier Polyimide Containing Carbazole Moiety: Synthesis, Gas Barrier Properties, and Molecular Simulations, Polymers 12 (2020) 204 | DOI 10.3390/polym12092048 | journal |
| [6] | Influence of deposition temperature on microstructure and gas-barrier properties of Al2O3 prepared by plasma-enhanced atomic layer deposition on a pol | DOI 10.1039/d3ra00121k | journal |
| [7] | Influence of Type of Cross-Linking Agent on Structure and Transport Properties of Polydecylmethylsiloxane (Rao et al. 2007, J. Membr. Sci. 303, 132-13 | DOI 10.3390/polym15224436 | journal |
| [8] | Pre-grafted Group on PE Surface by DBD Plasma and Its Influence on the Oxygen Permeation with Coated SiOx (Li H, Yang L, Wang Z, Liu Z, Chen Q.) | DOI 10.3390/molecules24040780 | journal |
| [9] | Water Vapor Permeation in Plastics (PNNL-26070), Table 4.3 — Some Water Vapor Permeability Coefficients [Bhadha 1999] | https://www.pnnl.gov/main/publications/external/technical_reports/PNNL-26070.pdf | other |
| [10] | Kapton Summary of Properties — Table 10. Chemical Properties of Kapton Type HN Film, 25 um (1 mil) | https://www.qnityelectronics.com/content/dam/electronics/amer/us/en/electronics/public/documents/en/EI-10142_K | datasheet |
| [11] | DuPont Kapton Polyimide Film - General Specifications (Reorder No. H-38492-2), Table 10 Chemical Properties of Kapton Type HN Film, 25 um (1 mil) | https://www.professionalplastics.com/professionalplastics/content/KaptonGeneral.pdf | datasheet |
| [12] | UPILEX-RN High elongation polyimide film — Specialty Products data sheet, Table-2 Thermal Properties | https://www.spacematdb.com/spacemat/manudatasheets/UpilexRN-566.pdf | datasheet |
| [13] | UBE UPILEX-S Polyimide Film Technical Data Sheet (UPILEX-25S, Tables 1/2/4-1) | https://www.spacematdb.com/spacemat/manudatasheets/UPILEXS%20Data%20sheet.pdf | datasheet |
| [14] | Chemical Vapour Deposition Graphene-PMMA Nanolaminates for Flexible Gas Barrier | DOI 10.3390/membranes12060611 | journal |
| [15] | Gas transport properties of poly(n-alkyl acrylate) blends and modeling of modified atmosphere storage using selective and non-selective membranes (B. | https://repositories.lib.utexas.edu/server/api/core/bitstreams/57695eb4-74ec-4a1a-b808-6b126bcfe936/content | other |
| [16] | SCS Parylene Properties (High performance conformal coatings) | https://nrf.aux.eng.ufl.edu/_files/documents/176.pdf | datasheet |
| [17] | Organic Polymer Hosts for Triplet-Triplet Annihilation Upconversion Systems (Macromolecules 2021, 54, 5, 2255-2270) — 본문이 Mogri Z.; Paul D. R. Polymer | DOI 10.1021/acs.macromol.1c00133 | journal |
| [18] | Toray Lumirror 기술정보 — Physical and Thermal Properties (샘플 #25 / 25 µm) | https://www.films.toray/en/technical/lumirror/lum_002.html | datasheet |
| [19] | Synergistic Enhancement of Oxygen Permeability in Silane-Modified Hydrogel Networks for Advanced Ophthalmic Applications (Gels 2025, 11, 987) | DOI 10.3390/gels11120987 | journal |
| [20] | GL-AE — GL FILM (Transparent Barrier Film) standard specifications | https://www.toppan-usa.com/products/gl-ae/ | datasheet |
| [21] | GL-AEC-F — GL FILM (Transparent Barrier Film) standard specifications | https://www.toppan-usa.com/products/gl-aec-f/ | datasheet |
| [22] | GL-ARH — GL FILM (Transparent Barrier Film) standard specifications | https://www.toppan-usa.com/products/gl-arh/ | datasheet |
| [23] | GL-BP-F — GL FILM (Transparent Barrier Film) standard specifications | https://www.toppan-usa.com/products/gl-bp-f/ | datasheet |
| [24] | GL-RD — GL FILM (Transparent Barrier Film) standard specifications | https://www.toppan-usa.com/products/gl-rd/ | datasheet |
| [25] | GX-P-F — GL FILM (Transparent Barrier Film) standard specifications | https://www.toppan-usa.com/products/gx-p-f/ | datasheet |
| [26] | Effect of Network Structure Modifications on the Light Gas Transport Properties of Cross-linked Poly(ethylene oxide) Membranes (V. A. Kusuma, PhD diss | https://repositories.lib.utexas.edu/server/api/core/bitstreams/49adec55-6fe8-44ad-b33c-13004449f4bd/content | other |

### 활성화에너지 Ea  (J/mol)  —  26건

| 재료 | 값 | 등급 | 조건 | 출처 |
| --- | --- | --- | --- | --- |
| PA14(45)/PA18(55) 블렌드 (poly(n-tetradecyl acrylate)/p | 50.21 kJ/mol | t3 | species=O2, state=blend, effective (융해구간 포함), process=O2 permeation, temperature_range=5 – 45 oC | [1] |
| PA14(50)/PA16(50) 블렌드 (poly(n-tetradecyl acrylate)/p | 63.6 kJ/mol | t3 | species=O2, state=blend, effective (융해구간 포함), process=O2 permeation, temperature_range=5 – 35 oC | [1] |
| PA14(75)/PA16(25) 블렌드 (poly(n-tetradecyl acrylate)/p | 69.04 kJ/mol | t3 | species=O2, state=blend, effective (융해구간 포함), process=O2 permeation, temperature_range=5 – 35 oC | [1] |
| PA16(50)/PA18(50) 블렌드 (poly(n-hexadecyl acrylate)/po | 56.9 kJ/mol | t3 | species=O2, state=blend, effective (융해구간 포함), process=O2 permeation, temperature_range=5 – 45 oC | [1] |
| PA16(50)/PA18(50) 블렌드 (poly(n-hexadecyl acrylate)/po | 36.82 kJ/mol | t3 | species=O2, state=solid (semi-crystalline blend), process=O2 permeation, cooling_rate_C_per_min=0.1, thermal_h… | [1] |
| PA16(50)/PA18(50) 블렌드 (poly(n-hexadecyl acrylate)/po | 40.59 kJ/mol | t3 | species=O2, state=solid (semi-crystalline blend), process=O2 permeation, cooling_rate_C_per_min=1.0, thermal_h… | [1] |
| PA16(50)/PA18(50) 블렌드 (poly(n-hexadecyl acrylate)/po | 38.49 kJ/mol | t3 | species=O2, state=intermediate (semi-crystalline blend), process=O2 permeation, cooling_rate_C_per_min=0.1, th… | [1] |
| PA16(50)/PA18(50) 블렌드 (poly(n-hexadecyl acrylate)/po | 46.44 kJ/mol | t3 | species=O2, state=intermediate (semi-crystalline blend), process=O2 permeation, cooling_rate_C_per_min=1.0, th… | [1] |
| PI Base Film — Kapton HN (DuPont) | 40.6 kJ/mol | t1 | mechanism=moisture diffusion (H2O in polyimide film) | [2] |
| Poly(decyl acrylate) (PA 10, n-alkyl acrylate homopo | 30.96 kJ/mol | t3 | species=O2, state=amorphous (Ea), process=O2 permeation | [3] |
| Poly(docosyl acrylate) (PA 22, n-alkyl acrylate homo | 16.74 kJ/mol | t3 | species=O2, state=molten / amorphous (Ea), process=O2 permeation, side_chain_carbons=22 | [3] |
| Poly(docosyl acrylate) (PA 22, n-alkyl acrylate homo | 40.59 kJ/mol | t3 | species=O2, state=semi-crystalline (Ec), process=O2 permeation, side_chain_carbons=22 | [3] |
| Poly(dodecyl acrylate) (PA 12, n-alkyl acrylate homo | 29.71 kJ/mol | t3 | species=O2, state=molten / amorphous (Ea), process=O2 permeation, side_chain_carbons=12 | [3] |
| Poly(dodecyl acrylate) (PA 12, n-alkyl acrylate homo | 46.02 kJ/mol | t3 | species=O2, state=semi-crystalline (Ec), process=O2 permeation, side_chain_carbons=12 | [3] |
| Poly(hexadecyl acrylate) (PA 16, n-alkyl acrylate ho | 39.33 kJ/mol | t3 | species=O2, state=semi-crystalline solid, process=O2 permeation, temperature_range=2 – 20 oC, side_chain_carbo… | [1] |
| Poly(hexyl acrylate) (PA 6, n-alkyl acrylate homopol | 28.45 kJ/mol | t3 | species=O2, state=amorphous (Ea), process=O2 permeation | [3] |
| Poly(octadecyl acrylate) (PA 18, n-alkyl acrylate ho | 21.76 kJ/mol | t3 | species=O2, state=molten / amorphous (Ea), process=O2 permeation, side_chain_carbons=18 | [3] |
| Poly(octadecyl acrylate) (PA 18, n-alkyl acrylate ho | 44.35 kJ/mol | t3 | species=O2, state=semi-crystalline (Ec), process=O2 permeation, side_chain_carbons=18 | [3] |
| Poly(octadecyl acrylate) (PA 18, n-alkyl acrylate ho | 46.02 kJ/mol | t3 | species=O2, state=semi-crystalline solid, process=O2 permeation, temperature_range=30 – 40 oC, side_chain_carb… | [1] |
| Poly(octadecyl acrylate) (PA 18, n-alkyl acrylate ho | 33.47 kJ/mol | t3 | species=O2, state=solid (semi-crystalline), process=O2 permeation, cooling_rate_C_per_min=0.1, side_chain_carb… | [1] |
| Poly(octadecyl acrylate) (PA 18, n-alkyl acrylate ho | 39.33 kJ/mol | t3 | species=O2, state=solid (semi-crystalline), process=O2 permeation, cooling_rate_C_per_min=1.0, side_chain_carb… | [1] |
| Poly(tetradecyl acrylate) (PA 14, n-alkyl acrylate h | 23.85 kJ/mol | t3 | species=O2, state=molten / amorphous (Ea), process=O2 permeation, side_chain_carbons=14 | [3] |
| Poly(tetradecyl acrylate) (PA 14, n-alkyl acrylate h | 36.4 kJ/mol | t3 | species=O2, state=semi-crystalline (Ec), process=O2 permeation, side_chain_carbons=14 | [3] |
| Poly(tetradecyl acrylate) (PA 14, n-alkyl acrylate h | 35.56 kJ/mol | t3 | species=O2, state=semi-crystalline solid, process=O2 permeation, temperature_range=2 – 12 oC, side_chain_carbo… | [1] |
| Polyimide gas separation membrane (UBE UMS-A2 module | 31.54 kJ/mol | t1 | species=O2, process=O2 diffusion, temperature_range_K=308-328, model=partial immobilization model, Arrhenius f… | [4] |
| XLPEGDA-80 (UV-cured PEGDA network, prepolymer 80 wt | 52 kJ/mol | t3 | species=O2, cure_state=fully cured (3차원 네트워크, sol 무시할 수준), process=O2 permeation, temperature_range_C=-20 to 4… | [5] |

출처

| # | 제목 | DOI / URL | 종류 |
| --- | --- | --- | --- |
| [1] | Gas transport properties of poly(n-alkyl acrylate) blends and modeling of modified atmosphere storage using selective and non-selective membranes (B. | https://repositories.lib.utexas.edu/server/api/core/bitstreams/57695eb4-74ec-4a1a-b808-6b126bcfe936/content | other |
| [2] | Role of filler and its heterostructure on moisture sorption mechanisms in polyimide films | DOI 10.1038/s41598-018-35181-1 | journal |
| [3] | Physical Properties of Poly (n-alkyl acrylate) Copolymers (K. A. O'Leary, PhD dissertation, The University of Texas at Austin, 2005; supervisor D. R. | https://repositories.lib.utexas.edu/server/api/core/bitstreams/b50f3cf2-2ce3-4e44-aba8-a120bd4e0003/content | other |
| [4] | Transport of Carbon Dioxide, Methane, Oxygen and Nitrogen in a Glassy Polyimide Membrane | DOI 10.3390/molecules30234524 | journal |
| [5] | Solubility selective membrane materials for carbon dioxide removal from mixtures with light gases (H. Lin, PhD dissertation, The University of Texas a | https://repositories.lib.utexas.edu/server/api/core/bitstreams/3fda6a29-fd3c-445b-b9dc-187caa9cb46a/content | other |

## 4.2  Stern-Volmer 소광

### 여기수명 τ₀  (s)  —  95건

| 재료 | 값 | 등급 | 조건 | 출처 |
| --- | --- | --- | --- | --- |
| 2BOCzSi blue emitter/host (bis boron-oxygen fused ca | 0.86 µs | t1 | matrix=oxygen-free toluene solution, atmosphere=oxygen-free, term=delayed, temperature_C=25 | [1] |
| 3CzCCN deep-blue TADF emitter (tri-carbazolyl carbaz | 3.8 ns | t1 | matrix=mCBP host film (10 wt%), atmosphere=vacuum, term=prompt, temperature_C=25 | [2] |
| 3CzCCN deep-blue TADF emitter (tri-carbazolyl carbaz | 180 µs | t1 | matrix=mCBP host film (10 wt%), atmosphere=vacuum, term=delayed, temperature_C=25 | [2] |
| 3MeCzCCN deep-blue TADF emitter (tri-methylcarbazoly | 5.1 ns | t1 | matrix=mCBP host film (10 wt%), atmosphere=vacuum, term=prompt, temperature_C=25 | [2] |
| 3MeCzCCN deep-blue TADF emitter (tri-methylcarbazoly | 47 µs | t1 | matrix=mCBP host film (10 wt%), atmosphere=vacuum, term=delayed, temperature_C=25 | [2] |
| 3Ph2CzCzBN blue TADF emitter (3,6-diphenylcarbazole/ | 3.7 ns | t1 | matrix=degassed toluene solution (1e-5 M), atmosphere=degassed, term=prompt, temperature_C=25 | [3] |
| 3Ph2CzCzBN blue TADF emitter (3,6-diphenylcarbazole/ | 10 µs | t1 | matrix=degassed toluene solution (1e-5 M), atmosphere=degassed, term=delayed, temperature_C=25 | [3] |
| 3PhCzCCN deep-blue TADF emitter (tri-phenylcarbazoly | 6.2 ns | t1 | matrix=mCBP host film (10 wt%), atmosphere=vacuum, term=prompt, temperature_C=25 | [2] |
| 3PhCzCCN deep-blue TADF emitter (tri-phenylcarbazoly | 34 µs | t1 | matrix=mCBP host film (10 wt%), atmosphere=vacuum, term=delayed, temperature_C=25 | [2] |
| 4CzBN blue TADF emitter (4-carbazolyl benzonitrile) | 1.6 ns | t1 | matrix=degassed toluene solution (1e-5 M), atmosphere=degassed, term=prompt, temperature_C=25 | [3] |
| 4CzBN blue TADF emitter (4-carbazolyl benzonitrile) | 50 µs | t1 | matrix=degassed toluene solution (1e-5 M), atmosphere=degassed, term=delayed, temperature_C=25 | [3] |
| Ac-PM deep-blue TADF emitter (9,9-dimethylacridan-ph | 11 ns | t1 | matrix=PPF host film (18 wt%), atmosphere=vacuum, term=prompt, temperature_C=25 | [4] |
| Ac-PM deep-blue TADF emitter (9,9-dimethylacridan-ph | 78 µs | t1 | matrix=PPF host film (18 wt%), atmosphere=vacuum, term=delayed, temperature_C=25 | [4] |
| BOCzSi blue emitter/host (boron-oxygen fused carbazo | 0.43 µs | t1 | matrix=oxygen-free toluene solution, atmosphere=oxygen-free, term=delayed, temperature_C=25 | [1] |
| DBCz-Mes BT.2020 blue multi-resonance emitter (mesit | 4.7 ns | t1 | matrix=degassed toluene solution (1e-5 M), atmosphere=degassed, term=prompt, temperature_K=300 | [5] |
| DBCz-Mes BT.2020 blue multi-resonance emitter (mesit | 80 µs | t1 | matrix=degassed toluene solution (1e-5 M), atmosphere=degassed, term=delayed, temperature_K=300 | [5] |
| DMAC-DPO blue emitter (dimethylacridan phenyl-diphen | 7 ns | t1 | matrix=toluene solution, atmosphere=N2-sparged (논문 각주 f가 tau_DF에 대해서만 N2-sparged를 명시 — tau_PF 분위기는 미기재), term=… | [6] |
| DMAC-F2DPO sky-blue TADF emitter (dimethylacridan di | 8.8 ns | t1 | matrix=nitrogen-sparged toluene solution, atmosphere=N2, term=prompt, temperature_C=25 | [7] |
| DMAC-F2DPO sky-blue TADF emitter (dimethylacridan di | 179 µs | t1 | matrix=nitrogen-sparged toluene solution, atmosphere=N2, term=delayed, temperature_C=25 | [7] |
| FIrpic blue phosphorescent dopant (bis[2-(4,6-difluo | 1.82 µs | t1 | matrix=degassed CH2Cl2 solution (~2e-5 M), atmosphere=degassed | [8] |
| H2TPP free-base porphyrin dye (5,10,15,20-tetrapheny | 286 µs | t1 | matrix=deaerated toluene solution (~1e-6 M), atmosphere=deaerated, term=triplet, temperature_C=25 | [9] |
| H2TPP free-base porphyrin dye (5,10,15,20-tetrapheny | 0.196 µs | t1 | matrix=non-degassed (air-equilibrated) toluene solution (~1e-6 M), atmosphere=air, term=triplet, quencher=O2, … | [9] |
| ITX photoinitiator (2-isopropylthioxanthone) | 2.7 µs | t1 | matrix=MeCN (acetonitrile), atmosphere=N2-purged (용액 10분 이상 + 헤드스페이스 5분 이상), term=triplet, temperature_C=미기재 —… | [10] |
| ITX photoinitiator (2-isopropylthioxanthone) | 5.9 µs | t1 | matrix=iPrOH (isopropanol), atmosphere=N2-purged (용액 10분 이상 + 헤드스페이스 5분 이상), term=triplet, temperature_C=미기재 —… | [10] |
| ITX photoinitiator (2-isopropylthioxanthone) | 37.1 µs | t1 | matrix=PEG (poly(ethylene glycol)-400), atmosphere=N2-purged (용액 10분 이상 + 헤드스페이스 5분 이상), term=triplet, tempera… | [10] |
| ITX photoinitiator (2-isopropylthioxanthone) | 25.8 µs | t1 | matrix=ethylene glycol, atmosphere=N2-purged (용액 10분 이상 + 헤드스페이스 5분 이상), term=triplet, temperature_C=미기재 — 논문이… | [10] |
| ITX photoinitiator (2-isopropylthioxanthone) | 1.6 µs | t1 | matrix=glyme (1,2-dimethoxyethane), atmosphere=N2-purged (용액 10분 이상 + 헤드스페이스 5분 이상), term=triplet, temperature… | [10] |
| Ir [3+2+1] piq-Br red phosphor (bis-NHC pincer / 1-p | 4.46 µs | t1 | matrix=degassed CH2Cl2 solution (~2e-5 M), atmosphere=degassed | [8] |
| Ir [3+2+1] piq-CN red phosphor (bis-NHC pincer / 1-p | 11.2 µs | t1 | matrix=degassed CH2Cl2 solution (~2e-5 M), atmosphere=degassed | [8] |
| Ir [3+2+1] piq-OCN red phosphor (bis-NHC pincer / 1- | 3.9 µs | t1 | matrix=degassed CH2Cl2 solution (~2e-5 M), atmosphere=degassed | [8] |
| Ir(pphen)2-coumarin dyad 3c deep-red phosphor (cyclo | 2.7 µs | t1 | matrix=CH2Cl2 solution, atmosphere=degassed (O2-free), temperature_k=293 | [11] |
| Ir(ppy)2(acac) green phosphorescent dopant (bis(2-ph | 0.73 µs | t1 | matrix=degassed CH2Cl2 solution (~2e-5 M), atmosphere=degassed | [8] |
| Ir-containing polynorbornene P1 red phosphor (water- | 1.5 µs | t1 | matrix=aqueous solution, atmosphere=degassed | [12] |
| Ir-containing polynorbornene P1 red phosphor (water- | 1.1 µs | t1 | matrix=aqueous solution, atmosphere=aerated, quencher=O2 | [12] |
| Ir-containing polynorbornene P3 red phosphor (water- | 1.5 µs | t1 | matrix=aqueous solution, atmosphere=degassed | [12] |
| Ir-containing polynorbornene P3 red phosphor (water- | 1.3 µs | t1 | matrix=aqueous solution, atmosphere=aerated, quencher=O2 | [12] |
| MFAc-PM deep-blue TADF emitter (spiroacridine-phenyl | 13 ns | t1 | matrix=PPF host film (18 wt%), atmosphere=vacuum, term=prompt, temperature_C=25 | [4] |
| MFAc-PM deep-blue TADF emitter (spiroacridine-phenyl | 45 µs | t1 | matrix=PPF host film (18 wt%), atmosphere=vacuum, term=delayed, temperature_C=25 | [4] |
| MFAc-PPM deep-blue TADF emitter (spiroacridine-diphe | 12 ns | t1 | matrix=PPF host film (18 wt%), atmosphere=vacuum, term=prompt, temperature_C=25 | [4] |
| MFAc-PPM deep-blue TADF emitter (spiroacridine-diphe | 38 µs | t1 | matrix=PPF host film (18 wt%), atmosphere=vacuum, term=delayed, temperature_C=25 | [4] |
| MXAc-PM deep-blue TADF emitter (spiroxanthene-acridi | 11 ns | t1 | matrix=PPF host film (18 wt%), atmosphere=vacuum, term=prompt, temperature_C=25 | [4] |
| MXAc-PM deep-blue TADF emitter (spiroxanthene-acridi | 70 µs | t1 | matrix=PPF host film (18 wt%), atmosphere=vacuum, term=delayed, temperature_C=25 | [4] |
| MXAc-PPM deep-blue TADF emitter (spiroxanthene-acrid | 11 ns | t1 | matrix=PPF host film (18 wt%), atmosphere=vacuum, term=prompt, temperature_C=25 | [4] |
| MXAc-PPM deep-blue TADF emitter (spiroxanthene-acrid | 40 µs | t1 | matrix=PPF host film (18 wt%), atmosphere=vacuum, term=delayed, temperature_C=25 | [4] |
| OLED Emitter Layer (Ir phosphor) | 1.95 µs | t3 | matrix=3 wt% Ir(ppy)3 doped film in 2-phenyl-4,6-bis(12-phenylindolo[2,3-a]carbazol-11-yl)-1,3,5-triazine host… | [13] |
| PdOEP red phosphorescent dopant (palladium(II) octae | 270 µs | t1 | matrix=deaerated toluene solution (~1e-6 M), atmosphere=deaerated, term=triplet, temperature_C=25 | [9] |
| PdOEP red phosphorescent dopant (palladium(II) octae | 0.241 µs | t1 | matrix=non-degassed (air-equilibrated) toluene solution (~1e-6 M), atmosphere=air, term=triplet, quencher=O2, … | [9] |
| PdTPP red phosphorescent dopant (palladium(II) meso- | 254 µs | t1 | matrix=deaerated toluene solution (~1e-6 M), atmosphere=deaerated, term=triplet, temperature_C=25 | [9] |
| PdTPP red phosphorescent dopant (palladium(II) meso- | 0.347 µs | t1 | matrix=non-degassed (air-equilibrated) toluene solution (~1e-6 M), atmosphere=air, term=triplet, quencher=O2, … | [9] |
| Pt(BPI-Et)(3-thienylacetylide) red Pt(II) phosphor / | 0.2 µs | t1 | matrix=toluene solution (1e-5 M), atmosphere=air-saturated (aerated), quencher=O2, temperature_C=20, excitatio… | [14] |
| Pt(BPI-Et)(3-thienylacetylide) red Pt(II) phosphor / | 0.8 µs | t1 | matrix=toluene solution (1e-5 M), atmosphere=deoxygenated (degassed), temperature_C=20, excitation_nm=510 | [14] |
| Pt(BPI-Et)(3-thienylacetylide) red Pt(II) phosphor / | 11.6 µs | t1 | matrix=2-MeTHF glass, atmosphere=rigid glass (no O2 diffusion), temperature_K=77, excitation_nm=510 | [14] |
| Pt(BPI-Et)(4-dimethylaminophenylacetylide) red Pt(II | 0.3 µs | t1 | matrix=toluene solution (1e-5 M), atmosphere=air-saturated (aerated), quencher=O2, temperature_C=20, excitatio… | [14] |
| Pt(BPI-Et)(4-dimethylaminophenylacetylide) red Pt(II | 1.1 µs | t1 | matrix=toluene solution (1e-5 M), atmosphere=deoxygenated (degassed), temperature_C=20, excitation_nm=510 | [14] |
| Pt(BPI-Et)(4-dimethylaminophenylacetylide) red Pt(II | 7.5 µs | t1 | matrix=2-MeTHF glass, atmosphere=rigid glass (no O2 diffusion), temperature_K=77, excitation_nm=510 | [14] |
| Pt(BPI-Et)(4-fluorophenylacetylide) red Pt(II) phosp | 0.3 µs | t1 | matrix=toluene solution (1e-5 M), atmosphere=air-saturated (aerated), quencher=O2, temperature_C=20, excitatio… | [14] |
| Pt(BPI-Et)(4-fluorophenylacetylide) red Pt(II) phosp | 1.5 µs | t1 | matrix=toluene solution (1e-5 M), atmosphere=deoxygenated (degassed), temperature_C=20, excitation_nm=510 | [14] |
| Pt(BPI-Et)(4-fluorophenylacetylide) red Pt(II) phosp | 12.1 µs | t1 | matrix=2-MeTHF glass, atmosphere=rigid glass (no O2 diffusion), temperature_K=77, excitation_nm=510 | [14] |
| Pt(BPI-Et)(4-methoxyphenylacetylide) red Pt(II) phos | 0.1 µs | t1 | matrix=toluene solution (1e-5 M), atmosphere=air-saturated (aerated), quencher=O2, temperature_C=20, excitatio… | [14] |
| Pt(BPI-Et)(4-methoxyphenylacetylide) red Pt(II) phos | 0.2 µs | t1 | matrix=toluene solution (1e-5 M), atmosphere=deoxygenated (degassed), temperature_C=20, excitation_nm=510 | [14] |
| Pt(BPI-Et)(4-methoxyphenylacetylide) red Pt(II) phos | 11.2 µs | t1 | matrix=2-MeTHF glass, atmosphere=rigid glass (no O2 diffusion), temperature_K=77, excitation_nm=510 | [14] |
| Pt(BPI-Et)(phenylacetylide) red Pt(II) phosphor / TT | 0.3 µs | t1 | matrix=toluene solution (1e-5 M), atmosphere=air-saturated (aerated), quencher=O2, temperature_C=20, excitatio… | [14] |
| Pt(BPI-Et)(phenylacetylide) red Pt(II) phosphor / TT | 1.5 µs | t1 | matrix=toluene solution (1e-5 M), atmosphere=deoxygenated (degassed), temperature_C=20, excitation_nm=510 | [14] |
| Pt(BPI-Et)(phenylacetylide) red Pt(II) phosphor / TT | 12.1 µs | t1 | matrix=2-MeTHF glass, atmosphere=rigid glass (no O2 diffusion), temperature_K=77, excitation_nm=510 | [14] |
| PtOEP red phosphorescent dopant (platinum(II) octaet | 60.5 µs | t1 | matrix=polycaprolactone (PCL) nanofiber membrane, 1 wt% PtOEP, atmosphere=vacuum, temperature_C=24 | [15] |
| PtOEP red phosphorescent dopant (platinum(II) octaet | 6.2 µs | t1 | matrix=polycaprolactone (PCL) nanofiber membrane, 1 wt% PtOEP, atmosphere=air, quencher=O2, temperature_C=24 | [15] |
| PtOEP red phosphorescent dopant (platinum(II) octaet | 1.41 µs | t1 | matrix=polycaprolactone (PCL) nanofiber membrane, 1 wt% PtOEP, atmosphere=O2 atmosphere, quencher=O2, temperat… | [15] |
| PtOEP red phosphorescent dopant (platinum(II) octaet | 83.9 µs | t1 | matrix=polystyrene (PS) nanofiber membrane, 1 wt% PtOEP, atmosphere=vacuum, temperature_C=24 | [15] |
| PtOEP red phosphorescent dopant (platinum(II) octaet | 15.2 µs | t1 | matrix=polystyrene (PS) nanofiber membrane, 1 wt% PtOEP, atmosphere=air, quencher=O2, temperature_C=24 | [15] |
| PtOEP red phosphorescent dopant (platinum(II) octaet | 4.46 µs | t1 | matrix=polystyrene (PS) nanofiber membrane, 1 wt% PtOEP, atmosphere=O2 atmosphere, quencher=O2, temperature_C=… | [15] |
| PtOEP red phosphorescent dopant (platinum(II) octaet | 80.8 µs | t1 | matrix=polyurethane Tecophilic (TECO) nanofiber membrane, 1 wt% PtOEP, atmosphere=vacuum, temperature_C=24 | [15] |
| PtOEP red phosphorescent dopant (platinum(II) octaet | 11.1 µs | t1 | matrix=polyurethane Tecophilic (TECO) nanofiber membrane, 1 wt% PtOEP, atmosphere=air, quencher=O2, temperatur… | [15] |
| PtOEP red phosphorescent dopant (platinum(II) octaet | 3.2 µs | t1 | matrix=polyurethane Tecophilic (TECO) nanofiber membrane, 1 wt% PtOEP, atmosphere=O2 atmosphere, quencher=O2, … | [15] |
| PtOEP red phosphorescent dopant (platinum(II) octaet | 81.4 µs | t1 | matrix=poly(vinylidene fluoride-co-hexafluoropropylene) (PVDF-HFP) nanofiber membrane, 1 wt% PtOEP, atmosphere… | [15] |
| PtOEP red phosphorescent dopant (platinum(II) octaet | 62 µs | t1 | matrix=poly(vinylidene fluoride-co-hexafluoropropylene) (PVDF-HFP) nanofiber membrane, 1 wt% PtOEP, atmosphere… | [15] |
| PtOEP red phosphorescent dopant (platinum(II) octaet | 11.2 µs | t1 | matrix=poly(vinylidene fluoride-co-hexafluoropropylene) (PVDF-HFP) nanofiber membrane, 1 wt% PtOEP, atmosphere… | [15] |
| TXADO-spiro-DMACF deep-blue TADF emitter (thioxanthe | 3.8 ns | t1 | matrix=neat film, atmosphere=N2, term=prompt, temperature_C=25 | [16] |
| TXADO-spiro-DMACF deep-blue TADF emitter (thioxanthe | 106 µs | t1 | matrix=neat film, atmosphere=N2, term=delayed, temperature_C=25 | [16] |
| [Pt(L1)(acac)] cyclometalated Pt(II) orange-red phos | 0.267 µs | t1 | matrix=aerated toluene solution, atmosphere=air, term=triplet, quencher=O2, wavelength_nm=405, temperature_C=2… | [17] |
| [Pt(L1)(acac)] cyclometalated Pt(II) orange-red phos | 0.9 µs | t1 | matrix=deaerated toluene solution, atmosphere=deaerated, term=tau1, wavelength_nm=405, temperature_C=25 | [17] |
| [Pt(L1)(acac)] cyclometalated Pt(II) orange-red phos | 2.2 µs | t1 | matrix=deaerated toluene solution, atmosphere=deaerated, term=tau2, wavelength_nm=405, temperature_C=25 | [17] |
| [Pt(L2)(acac)] cyclometalated Pt(II) orange-red phos | 0.271 µs | t1 | matrix=aerated toluene solution, atmosphere=air, term=triplet, quencher=O2, wavelength_nm=405, temperature_C=2… | [17] |
| [Pt(L2)(acac)] cyclometalated Pt(II) orange-red phos | 1.3 µs | t1 | matrix=deaerated toluene solution, atmosphere=deaerated, term=tau1, wavelength_nm=405, temperature_C=25 | [17] |
| [Pt(L2)(acac)] cyclometalated Pt(II) orange-red phos | 2.3 µs | t1 | matrix=deaerated toluene solution, atmosphere=deaerated, term=tau2, wavelength_nm=405, temperature_C=25 | [17] |
| [Pt(L3)(acac)] cyclometalated Pt(II) orange-red phos | 0.304 µs | t1 | matrix=aerated toluene solution, atmosphere=air, term=triplet, quencher=O2, wavelength_nm=405, temperature_C=2… | [17] |
| [Pt(L3)(acac)] cyclometalated Pt(II) orange-red phos | 1.5 µs | t1 | matrix=deaerated toluene solution, atmosphere=deaerated, term=tau1, wavelength_nm=405, temperature_C=25 | [17] |
| [Pt(L3)(acac)] cyclometalated Pt(II) orange-red phos | 2.7 µs | t1 | matrix=deaerated toluene solution, atmosphere=deaerated, term=tau2, wavelength_nm=405, temperature_C=25 | [17] |
| [Pt(L4)(acac)] cyclometalated Pt(II) orange-red phos | 0.5 µs | t1 | matrix=aerated toluene solution, atmosphere=air, term=triplet, quencher=O2, wavelength_nm=405, temperature_C=2… | [17] |
| [Pt(L4)(acac)] cyclometalated Pt(II) orange-red phos | 1.4 µs | t1 | matrix=deaerated toluene solution, atmosphere=deaerated, term=tau1, wavelength_nm=405, temperature_C=25 | [17] |
| [Pt(L4)(acac)] cyclometalated Pt(II) orange-red phos | 2.6 µs | t1 | matrix=deaerated toluene solution, atmosphere=deaerated, term=tau2, wavelength_nm=405, temperature_C=25 | [17] |
| [Pt(L5)(acac)] cyclometalated Pt(II) orange-red phos | 0.277 µs | t1 | matrix=aerated toluene solution, atmosphere=air, term=triplet, quencher=O2, wavelength_nm=405, temperature_C=2… | [17] |
| [Pt(L5)(acac)] cyclometalated Pt(II) orange-red phos | 1.2 µs | t1 | matrix=deaerated toluene solution, atmosphere=deaerated, term=tau1, wavelength_nm=405, temperature_C=25 | [17] |
| [Pt(L5)(acac)] cyclometalated Pt(II) orange-red phos | 1.7 µs | t1 | matrix=deaerated toluene solution, atmosphere=deaerated, term=tau2, wavelength_nm=405, temperature_C=25 | [17] |
| pSFIAc1 narrowband deep-blue fluorescent emitter (sp | 7.7 ns | t1 | matrix=degassed toluene solution (1e-5 M), atmosphere=degassed, term=single-exponential fluorescence, temperat… | [18] |
| pSFIAc2 narrowband deep-blue fluorescent emitter (sp | 8 ns | t1 | matrix=degassed toluene solution (1e-5 M), atmosphere=degassed, term=single-exponential fluorescence, temperat… | [18] |

출처

| # | 제목 | DOI / URL | 종류 |
| --- | --- | --- | --- |
| [1] | Yuan et al., Complementarity fusion of boron-oxygen and carbazole blocks enables narrowband blue OLEDs with high performance, Nature Communications 16 | DOI 10.1038/s41467-025-65446-z | journal |
| [2] | Chan et al., Carbazole-2-carbonitrile as an acceptor in deep-blue thermally activated delayed fluorescence emitters for narrowing charge-transfer emis | DOI 10.1039/d2sc02478k | journal |
| [3] | Chan et al., Efficient and stable sky-blue delayed fluorescence organic light-emitting diodes with CIEy below 0.4, Nature Communications 9 (2018), Tab | DOI 10.1038/s41467-018-07482-6 | journal |
| [4] | Park et al., Pyrimidine-based twisted donor-acceptor delayed fluorescence molecules: a new universal platform for highly efficient blue electrolumines | DOI 10.1039/c6sc03793c | journal |
| [5] | Wang et al., Improving the stability and color purity of a BT.2020 blue multiresonance emitter by alleviating hydrogen repulsion, Science Advances 9 ( | DOI 10.1126/sciadv.adh1434 | journal |
| [6] | Cooper et al., Control of Singlet Emission Energy in a Diphenyloxadiazole Containing Fluorophore Leading To Thermally Activated Delayed Fluorescence | DOI 10.1021/acsomega.9b00825 | journal |
| [7] | Cooper et al., Control of Singlet Emission Energy in a Diphenyloxadiazole Containing Fluorophore Leading To Thermally Activated Delayed Fluorescence, | DOI 10.1021/acsomega.8b01979 | journal |
| [8] | Wu et al., Phosphorescent [3+2+1] coordinated Ir(iii) cyano complexes for achieving efficient phosphors and their application in OLED devices, Chem. S | DOI 10.1039/d1sc01426a | journal |
| [9] | Banaszek et al., Enhancing Photostability by Thermodynamic and Kinetic Factors: Free-Base and Palladium meso-Aryl-octaethylporphyrins, J. Phys. Chem. | DOI 10.1021/acs.jpcb.5c02423 | journal |
| [10] | Liaros et al., Elucidating complex triplet-state dynamics in the model system isopropylthioxanthone (iScience 25, 103600) — Supplemental Information, | DOI 10.1016/j.isci.2021.103600 | journal |
| [11] | Wu, Sutton, Halamicek, Xing, Bao, Teets, Cyclometalated iridium-coumarin ratiometric oxygen sensors: improved signal resolution and tunable dynamic ra | DOI 10.1039/d2sc02909j | journal |
| [12] | Bochkarev et al., Red Light-Emitting Water-Soluble Luminescent Iridium-Containing Polynorbornenes, Molecules 26 (2021) 6349, Tables 1 and 2 | DOI 10.3390/molecules26216349 | journal |
| [13] | Enhancing Horizontal Ratio of Transition Dipole Moment in Homoleptic Ir Complexes for High Outcoupling Efficiency of Organic Light-Emitting Diodes | DOI 10.1002/advs.202203903 | journal |
| [14] | Payce et al., Energy Upconversion Using Platinum(II)-BPI Photosensitizers, Inorg. Chem. 64 (2025) 24851-24864, Table 8 ('A Comparison of the Solvent D | DOI 10.1021/acs.inorgchem.5c04677 | journal |
| [15] | Ludacka et al., Luminescent Oxygen Sensor with Self-Sterilization Properties Based on Platinum(II)octaethylporphyrin in Polymeric Nanofibers, ACS Mate | DOI 10.1021/acsmaterialsau.4c00137 | journal |
| [16] | Rao et al., Achieving Deep-Blue Thermally Activated Delayed Fluorescence in Nondoped Organic Light-Emitting Diodes through a Spiro-Blocking Strategy, | DOI 10.1021/acsomega.8b03296 | journal |
| [17] | Fitzgerald et al., Organometallic Platinum(II) Photosensitisers that Demonstrate Ligand-Modulated Triplet-Triplet Annihilation Energy Upconversion Eff | DOI 10.1002/chem.202203241 | journal |
| [18] | Meng et al., Highly efficient and stable deep-blue OLEDs based on narrowband emitters featuring an orthogonal spiro-configured indolo[3,2,1-de]acridin | DOI 10.1039/d2sc01543a | journal |

### Stern-Volmer 상수 K_SV  (1/Pa)  —  6건

| 재료 | 값 | 등급 | 조건 | 출처 |
| --- | --- | --- | --- | --- |
| Ir(F2ppy)2(CNAr-dmp)(pyridyl-coumarin C-1) ratiometr | 0.0187515 | t1 | matrix=CH2Cl2 solution, atmosphere=O2 titration (variable pO2), quencher=O2, temperature_K=293 | [1] |
| Ir(F2ppy)2(pyridyl-coumarin C-1)2 ratiometric O2 sen | 0.00195016 | t1 | matrix=CH2Cl2 solution, atmosphere=O2 titration (variable pO2), quencher=O2, temperature_K=293 | [1] |
| Ir(F2ppy)2-bis(coumarin) dyad 5a phosphor (coumarin- | 0.00195016 | t1 | matrix=CH2Cl2 solution, quencher=O2, temperature_k=293 | [1] |
| Ir(F2ppy)2-coumarin dyad 3a phosphor (coumarin-centr | 0.0187515 | t1 | matrix=CH2Cl2 solution, quencher=O2, temperature_k=293 | [1] |
| Ir(pphen)2(CNAr-dmp)(pyridyl-coumarin C-1) ratiometr | 9.751e-05 | t1 | matrix=CH2Cl2 solution, atmosphere=O2 titration (variable pO2), quencher=O2, temperature_K=293 | [1] |
| Ir(pphen)2-coumarin dyad 3c deep-red phosphor (cyclo | 9.751e-05 | t1 | matrix=CH2Cl2 solution, quencher=O2, temperature_k=293 | [1] |

출처

| # | 제목 | DOI / URL | 종류 |
| --- | --- | --- | --- |
| [1] | Wu, Sutton, Halamicek, Xing, Bao, Teets, Cyclometalated iridium-coumarin ratiometric oxygen sensors: improved signal resolution and tunable dynamic ra | DOI 10.1039/d2sc02909j | journal |

### 소광 속도상수 k_q  (m³/(mol·s))  —  3건

| 재료 | 값 | 등급 | 조건 | 출처 |
| --- | --- | --- | --- | --- |
| Ir(pphen)2(CNAr-dmp)(pyridyl-coumarin C-1) ratiometr | 3.3e+05 | t1 | matrix=CH2Cl2 solution, atmosphere=O2 titration (variable pO2), quencher=O2, temperature_K=293 | [1] |
| Ir(pphen)2-coumarin dyad 3c deep-red phosphor (cyclo | 3.3e+05 | t2 | matrix=CH2Cl2 solution, quencher=O2, temperature_k=293 | [1] |
| Thioxanthone photoinitiator (TX) | 1e+06 | t3 | matrix=chloroform solution, quencher=O2, temperature_C=25, excitation_nm=355, grade_scope=class value — 측정 대상은… | [2] |

출처

| # | 제목 | DOI / URL | 종류 |
| --- | --- | --- | --- |
| [1] | Wu, Sutton, Halamicek, Xing, Bao, Teets, Cyclometalated iridium-coumarin ratiometric oxygen sensors: improved signal resolution and tunable dynamic ra | DOI 10.1039/d2sc02909j | journal |
| [2] | Rodrigues et al., Thioxanthone-Based Siloxane Photosensitizer for Cationic/Radical Photopolymerization and Photoinduced Sol-Gel Reactions, Molecules 2 | DOI 10.3390/molecules29010255 | journal |

### 광발광 양자수율 PLQY  (1)  —  42건

| 재료 | 값 | 등급 | 조건 | 출처 |
| --- | --- | --- | --- | --- |
| 3CzCCN deep-blue TADF emitter (tri-carbazolyl carbaz | 0.37 | t1 | matrix=toluene solution, atmosphere=degassed, temperature_C=25 | [1] |
| 3CzCCN deep-blue TADF emitter (tri-carbazolyl carbaz | 0.27 | t1 | matrix=toluene solution, atmosphere=air, quencher=O2, temperature_C=25 | [1] |
| 3CzCCN deep-blue TADF emitter (tri-carbazolyl carbaz | 0.4 | t1 | matrix=mCBP host film (10 wt%), atmosphere=N2, temperature_C=25 | [1] |
| 3MeCzCCN deep-blue TADF emitter (tri-methylcarbazoly | 0.59 | t1 | matrix=toluene solution, atmosphere=degassed, temperature_C=25 | [1] |
| 3MeCzCCN deep-blue TADF emitter (tri-methylcarbazoly | 0.21 | t1 | matrix=toluene solution, atmosphere=air, quencher=O2, temperature_C=25 | [1] |
| 3MeCzCCN deep-blue TADF emitter (tri-methylcarbazoly | 0.61 | t1 | matrix=mCBP host film (10 wt%), atmosphere=N2, temperature_C=25 | [1] |
| 3Ph2CzCzBN blue TADF emitter (3,6-diphenylcarbazole/ | 0.95 | t1 | matrix=toluene solution (1e-5 M), atmosphere=degassed, temperature_C=25 | [2] |
| 3Ph2CzCzBN blue TADF emitter (3,6-diphenylcarbazole/ | 0.16 | t1 | matrix=toluene solution (1e-5 M), atmosphere=air, quencher=O2, temperature_C=25 | [2] |
| 3PhCzCCN deep-blue TADF emitter (tri-phenylcarbazoly | 0.85 | t1 | matrix=toluene solution, atmosphere=degassed, temperature_C=25 | [1] |
| 3PhCzCCN deep-blue TADF emitter (tri-phenylcarbazoly | 0.32 | t1 | matrix=toluene solution, atmosphere=air, quencher=O2, temperature_C=25 | [1] |
| 3PhCzCCN deep-blue TADF emitter (tri-phenylcarbazoly | 0.72 | t1 | matrix=mCBP host film (10 wt%), atmosphere=N2, temperature_C=25 | [1] |
| 4CzBN blue TADF emitter (4-carbazolyl benzonitrile) | 0.63 | t1 | matrix=toluene solution (1e-5 M), atmosphere=degassed, temperature_C=25 | [2] |
| 4CzBN blue TADF emitter (4-carbazolyl benzonitrile) | 0.09 | t1 | matrix=toluene solution (1e-5 M), atmosphere=air, quencher=O2, temperature_C=25 | [2] |
| Ac-PM deep-blue TADF emitter (9,9-dimethylacridan-ph | 0.83 | t1 | matrix=PPF host film (18 wt%), atmosphere=N2, temperature_C=25 | [3] |
| DMAC-DPO blue emitter (dimethylacridan phenyl-diphen | 0.18 | t1 | matrix=toluene solution, atmosphere=N2, temperature_C=25 | [4] |
| DMAC-DPO blue emitter (dimethylacridan phenyl-diphen | 0.16 | t1 | matrix=toluene solution, atmosphere=air, quencher=O2, temperature_C=25 | [4] |
| DMAC-F2DPO sky-blue TADF emitter (dimethylacridan di | 0.24 | t1 | matrix=toluene solution, atmosphere=N2, temperature_C=25 | [4] |
| DMAC-F2DPO sky-blue TADF emitter (dimethylacridan di | 0.15 | t1 | matrix=toluene solution, atmosphere=air, quencher=O2, temperature_C=25 | [4] |
| FIrpic blue phosphorescent dopant (bis[2-(4,6-difluo | 0.69 | t1 | matrix=degassed CH2Cl2 solution (~2e-5 M), atmosphere=degassed | [5] |
| Ir [3+2+1] piq-Br red phosphor (bis-NHC pincer / 1-p | 0.6 | t1 | matrix=degassed CH2Cl2 solution (~2e-5 M), atmosphere=degassed | [5] |
| Ir [3+2+1] piq-CN red phosphor (bis-NHC pincer / 1-p | 0.49 | t1 | matrix=degassed CH2Cl2 solution (~2e-5 M), atmosphere=degassed | [5] |
| Ir [3+2+1] piq-OCN red phosphor (bis-NHC pincer / 1- | 0.62 | t1 | matrix=degassed CH2Cl2 solution (~2e-5 M), atmosphere=degassed | [5] |
| Ir-containing polynorbornene P1 red phosphor (water- | 0.1 | t1 | matrix=CH2Cl2 solution, atmosphere=degassed | [6] |
| Ir-containing polynorbornene P1 red phosphor (water- | 0.027 | t1 | matrix=CH2Cl2 solution, atmosphere=aerated, quencher=O2 | [6] |
| Ir-containing polynorbornene P1 red phosphor (water- | 0.038 | t1 | matrix=aqueous solution, atmosphere=degassed | [6] |
| Ir-containing polynorbornene P1 red phosphor (water- | 0.028 | t1 | matrix=aqueous solution, atmosphere=aerated, quencher=O2 | [6] |
| Ir-containing polynorbornene P3 red phosphor (water- | 0.093 | t1 | matrix=CH2Cl2 solution, atmosphere=degassed | [6] |
| Ir-containing polynorbornene P3 red phosphor (water- | 0.036 | t1 | matrix=CH2Cl2 solution, atmosphere=aerated, quencher=O2 | [6] |
| Ir-containing polynorbornene P3 red phosphor (water- | 0.027 | t1 | matrix=aqueous solution, atmosphere=degassed | [6] |
| Ir-containing polynorbornene P3 red phosphor (water- | 0.02 | t1 | matrix=aqueous solution, atmosphere=aerated, quencher=O2 | [6] |
| MFAc-PM deep-blue TADF emitter (spiroacridine-phenyl | 0.91 | t1 | matrix=PPF host film (18 wt%), atmosphere=N2, temperature_C=25 | [3] |
| MFAc-PPM deep-blue TADF emitter (spiroacridine-diphe | 0.87 | t1 | matrix=PPF host film (18 wt%), atmosphere=N2, temperature_C=25 | [3] |
| MXAc-PM deep-blue TADF emitter (spiroxanthene-acridi | 0.9 | t1 | matrix=PPF host film (18 wt%), atmosphere=N2, temperature_C=25 | [3] |
| MXAc-PPM deep-blue TADF emitter (spiroxanthene-acrid | 0.69 | t1 | matrix=PPF host film (18 wt%), atmosphere=N2, temperature_C=25 | [3] |
| OLED Emitter Layer (Ir phosphor) | 0.732 | t3 | matrix=3 wt% Ir(ppy)3 doped film in 2-phenyl-4,6-bis(12-phenylindolo[2,3-a]carbazol-11-yl)-1,3,5-triazine host… | [7] |
| TXADO-spiro-DMACF deep-blue TADF emitter (thioxanthe | 0.42 | t1 | matrix=neat film, atmosphere=N2, temperature_C=25 | [8] |
| TXADO-spiro-DMACF deep-blue TADF emitter (thioxanthe | 0.41 | t1 | matrix=TCTA host film (10 wt%), atmosphere=N2, temperature_C=25 | [8] |
| [Pt(L1)(acac)] cyclometalated Pt(II) orange-red phos | 0.219 | t1 | matrix=deaerated dichloromethane (DCM) solution, atmosphere=N2, wavelength_nm=440, temperature_C=25 | [9] |
| [Pt(L2)(acac)] cyclometalated Pt(II) orange-red phos | 0.321 | t1 | matrix=deaerated dichloromethane (DCM) solution, atmosphere=N2, wavelength_nm=440, temperature_C=25 | [9] |
| [Pt(L3)(acac)] cyclometalated Pt(II) orange-red phos | 0.371 | t1 | matrix=deaerated dichloromethane (DCM) solution, atmosphere=N2, wavelength_nm=440, temperature_C=25 | [9] |
| [Pt(L4)(acac)] cyclometalated Pt(II) orange-red phos | 0.343 | t1 | matrix=deaerated dichloromethane (DCM) solution, atmosphere=N2, wavelength_nm=440, temperature_C=25 | [9] |
| [Pt(L5)(acac)] cyclometalated Pt(II) orange-red phos | 0.271 | t1 | matrix=deaerated dichloromethane (DCM) solution, atmosphere=N2, wavelength_nm=440, temperature_C=25 | [9] |

출처

| # | 제목 | DOI / URL | 종류 |
| --- | --- | --- | --- |
| [1] | Chan et al., Carbazole-2-carbonitrile as an acceptor in deep-blue thermally activated delayed fluorescence emitters for narrowing charge-transfer emis | DOI 10.1039/d2sc02478k | journal |
| [2] | Chan et al., Efficient and stable sky-blue delayed fluorescence organic light-emitting diodes with CIEy below 0.4, Nature Communications 9 (2018), Tab | DOI 10.1038/s41467-018-07482-6 | journal |
| [3] | Park et al., Pyrimidine-based twisted donor-acceptor delayed fluorescence molecules: a new universal platform for highly efficient blue electrolumines | DOI 10.1039/c6sc03793c | journal |
| [4] | Cooper et al., Control of Singlet Emission Energy in a Diphenyloxadiazole Containing Fluorophore Leading To Thermally Activated Delayed Fluorescence, | DOI 10.1021/acsomega.8b01979 | journal |
| [5] | Wu et al., Phosphorescent [3+2+1] coordinated Ir(iii) cyano complexes for achieving efficient phosphors and their application in OLED devices, Chem. S | DOI 10.1039/d1sc01426a | journal |
| [6] | Bochkarev et al., Red Light-Emitting Water-Soluble Luminescent Iridium-Containing Polynorbornenes, Molecules 26 (2021) 6349, Tables 1 and 2 | DOI 10.3390/molecules26216349 | journal |
| [7] | Enhancing Horizontal Ratio of Transition Dipole Moment in Homoleptic Ir Complexes for High Outcoupling Efficiency of Organic Light-Emitting Diodes | DOI 10.1002/advs.202203903 | journal |
| [8] | Rao et al., Achieving Deep-Blue Thermally Activated Delayed Fluorescence in Nondoped Organic Light-Emitting Diodes through a Spiro-Blocking Strategy, | DOI 10.1021/acsomega.8b03296 | journal |
| [9] | Fitzgerald et al., Organometallic Platinum(II) Photosensitisers that Demonstrate Ligand-Modulated Triplet-Triplet Annihilation Energy Upconversion Eff | DOI 10.1002/chem.202203241 | journal |

## 4.3  UV 리셋 — 잔류 개시제 라디칼의 산소 소거

### 몰흡광계수 ε  (m²/mol)  —  21건

| 재료 | 값 | 등급 | 조건 | 출처 |
| --- | --- | --- | --- | --- |
| Benzophenone photoinitiator (Type II) | 2200 | t3 | wavelength_nm=253 | [1] |
| Benzophenone photoinitiator (Type II) | 25 | t3 | wavelength_nm=363 | [1] |
| ITX photoinitiator (2-isopropylthioxanthone) | 650 | t3 | wavelength_nm=386 | [1] |
| ITX photoinitiator (2-isopropylthioxanthone) | 390 | t3 | wavelength_nm=395 | [1] |
| ITX photoinitiator (2-isopropylthioxanthone) | 100 | t3 | wavelength_nm=405 | [1] |
| Irgacure 2959 photoinitiator (2-hydroxy-4'-(2-hydrox | 0.4 | t3 | wavelength_nm=365 | [2] |
| Irgacure 2959 photoinitiator (2-hydroxy-4'-(2-hydrox | 0.2 | t3 | wavelength_nm=405 | [3] |
| Irgacure 819 photoinitiator (BAPO, bis-acylphosphine | 66 | t3 | wavelength_nm=395 | [1] |
| Irgacure 819 photoinitiator (BAPO, bis-acylphosphine | 87 | t3 | wavelength_nm=370 | [4] |
| Irgacure TPO photoinitiator (diphenyl(2,4,6-trimethy | 54.5 | t1 | wavelength_nm=395, solvent=dichloromethane (CH2Cl2) | [5] |
| Irgacure TPO photoinitiator (diphenyl(2,4,6-trimethy | 57 | t3 | wavelength_nm=380 | [1] |
| Irgacure TPO photoinitiator (diphenyl(2,4,6-trimethy | 51 | t3 | wavelength_nm=385 | [1] |
| Irgacure TPO photoinitiator (diphenyl(2,4,6-trimethy | 2 | t3 | wavelength_nm=420 | [1] |
| Irgacure TPO photoinitiator (diphenyl(2,4,6-trimethy | 52 | t3 | wavelength_nm=380 | [4] |
| Irgacure TPO photoinitiator (diphenyl(2,4,6-trimethy | 68 | t3 | wavelength_nm=365 | [2] |
| Pt(BPI-Et)(3-thienylacetylide) red Pt(II) phosphor / | 962 | t1 | wavelength_nm=490, solvent=chloroform (CHCl3), concentration_M=1e-05 | [6] |
| Pt(BPI-Et)(4-dimethylaminophenylacetylide) red Pt(II | 739 | t1 | wavelength_nm=487, solvent=chloroform (CHCl3), concentration_M=1e-05 | [6] |
| Pt(BPI-Et)(4-fluorophenylacetylide) red Pt(II) phosp | 894 | t1 | wavelength_nm=492, solvent=chloroform (CHCl3), concentration_M=1e-05 | [6] |
| Pt(BPI-Et)(4-methoxyphenylacetylide) red Pt(II) phos | 1065 | t1 | wavelength_nm=489, solvent=chloroform (CHCl3), concentration_M=1e-05 | [6] |
| Pt(BPI-Et)(phenylacetylide) red Pt(II) phosphor / TT | 1065 | t1 | wavelength_nm=490, solvent=chloroform (CHCl3), concentration_M=1e-05 | [6] |
| Thioxanthone photoinitiator (TX) | 530 | t3 | wavelength_nm=380 | [1] |

출처

| # | 제목 | DOI / URL | 종류 |
| --- | --- | --- | --- |
| [1] | High-Performance Photoinitiating Systems for LED-Induced Photopolymerization | DOI 10.3390/polym15020342 | journal |
| [2] | Photocrosslinkable Biomaterials for 3D Bioprinting: Mechanisms, Recent Advances, and Future Prospects | DOI 10.3390/ijms252312567 | journal |
| [3] | 3D printing of highly stretchable hydrogel with diverse UV curable polymers | DOI 10.1126/sciadv.aba4261 | journal |
| [4] | Photoinitiators for Medical Applications - The Latest Advances | DOI 10.3390/molecules29163898 | journal |
| [5] | Beyond absorption: online photoreactor mass spectrometry assessment of new acylphosphine oxide photoinitiators | DOI 10.1039/d5sc03654b | journal |
| [6] | Payce et al., Energy Upconversion Using Platinum(II)-BPI Photosensitizers, Inorg. Chem. 64 (2025) 24851-24864, Table 8 ('A Comparison of the Solvent D | DOI 10.1021/acs.inorgchem.5c04677 | journal |

## 4.4  UV·외광의 내부 도달 경로

### 분광 투과율 T  (1)  —  78건

| 재료 | 값 | 등급 | 조건 | 출처 |
| --- | --- | --- | --- | --- |
| Color Filter Resin (pigment) | 0.8 | t4 | filter_color=blue, spectral_region=passband peak, assumption=True | [1] |
| Color Filter Resin (pigment) | 0.92 | t4 | wavelength_nm=550, color=green pixel, assumption=True | [2] |
| Color Filter Resin (pigment) | 0.9483 | t1 | detail=Pigment-dispersed yellow color filter resin (commercial CF solution, SynthEdge Advanced Materials), 1 u… | [3] |
| Color Filter Resin (pigment) | 0.0084 | t1 | detail=Same pigment-dispersed yellow color filter resin, 1 um film, at wavelength 446 nm (blue stop-band) | [3] |
| Color filter blue pigment layer with IR-cut dye (CMO | 0.77 | t1 | wavelength_nm=450, color=blue, thickness_um=1.0, pigment_type=pigment, sample=Example 17 | [4] |
| Color filter blue pigment layer with IR-cut dye (CMO | 0.11 | t1 | wavelength_nm=700, color=blue, thickness_um=1.0, pigment_type=pigment, sample=Example 17 | [4] |
| Color filter blue pigment layer with IR-cut dye (CMO | 0.76 | t1 | wavelength_nm=910, color=blue, thickness_um=1.0, pigment_type=pigment, sample=Example 17 | [4] |
| Color filter blue pigment layer with IR-cut dye (CMO | 0.73 | t1 | wavelength_nm=450, color=blue, thickness_um=0.9, pigment_type=pigment, sample=Example 25 | [4] |
| Color filter blue pigment layer with IR-cut dye (CMO | 0.07 | t1 | wavelength_nm=700, color=blue, thickness_um=0.9, pigment_type=pigment, sample=Example 25 | [4] |
| Color filter blue pigment layer with IR-cut dye (CMO | 0.81 | t1 | wavelength_nm=910, color=blue, thickness_um=0.9, pigment_type=pigment, sample=Example 25 | [4] |
| Color filter blue pigment layer with IR-cut dye (CMO | 0.8 | t1 | wavelength_nm=450, color=blue, thickness_um=0.9, pigment_type=pigment, sample=Example 26 | [4] |
| Color filter blue pigment layer with IR-cut dye (CMO | 0.11 | t1 | wavelength_nm=700, color=blue, thickness_um=0.9, pigment_type=pigment, sample=Example 26 | [4] |
| Color filter blue pigment layer with IR-cut dye (CMO | 0.85 | t1 | wavelength_nm=910, color=blue, thickness_um=0.9, pigment_type=pigment, sample=Example 26 | [4] |
| Color filter green pigment PG58 (halogenated zinc ph | 0.00606 | t1 | wavelength_nm=400, color=green, pigment_type=pigment (C.I. Pigment Green 58), sample=Example 1, form=0.005 wt%… | [5] |
| Color filter green pigment PG58 (halogenated zinc ph | 0.20909 | t1 | wavelength_nm=450, color=green, pigment_type=pigment (C.I. Pigment Green 58), sample=Example 1, form=0.005 wt%… | [5] |
| Color filter green pigment PG58 (halogenated zinc ph | 0.86269 | t1 | wavelength_nm=533, color=green, pigment_type=pigment (C.I. Pigment Green 58), sample=Example 1, form=0.005 wt%… | [5] |
| Color filter green pigment PG58 (halogenated zinc ph | 0.0094 | t1 | wavelength_nm=400, color=green, pigment_type=pigment (C.I. Pigment Green 58), sample=Example 2, form=0.005 wt%… | [5] |
| Color filter green pigment PG58 (halogenated zinc ph | 0.22443 | t1 | wavelength_nm=450, color=green, pigment_type=pigment (C.I. Pigment Green 58), sample=Example 2, form=0.005 wt%… | [5] |
| Color filter green pigment PG58 (halogenated zinc ph | 0.87381 | t1 | wavelength_nm=533, color=green, pigment_type=pigment (C.I. Pigment Green 58), sample=Example 2, form=0.005 wt%… | [5] |
| Color filter green pigment PG58 (halogenated zinc ph | 0.00276 | t1 | wavelength_nm=400, color=green, pigment_type=pigment (C.I. Pigment Green 58), sample=Example 3, form=0.005 wt%… | [5] |
| Color filter green pigment PG58 (halogenated zinc ph | 0.13173 | t1 | wavelength_nm=450, color=green, pigment_type=pigment (C.I. Pigment Green 58), sample=Example 3, form=0.005 wt%… | [5] |
| Color filter green pigment PG58 (halogenated zinc ph | 0.84721 | t1 | wavelength_nm=528, color=green, pigment_type=pigment (C.I. Pigment Green 58), sample=Example 3, form=0.005 wt%… | [5] |
| Color filter green pigment PG58 (halogenated zinc ph | 0.02843 | t1 | wavelength_nm=400, color=green, pigment_type=pigment (C.I. Pigment Green 58), sample=Comparative Example, form… | [5] |
| Color filter green pigment PG58 (halogenated zinc ph | 0.22299 | t1 | wavelength_nm=450, color=green, pigment_type=pigment (C.I. Pigment Green 58), sample=Comparative Example, form… | [5] |
| Color filter green pigment PG58 (halogenated zinc ph | 0.85059 | t1 | wavelength_nm=539, color=green, pigment_type=pigment (C.I. Pigment Green 58), sample=Comparative Example, form… | [5] |
| Color filter green pigment PG58 (halogenated zinc ph | 0.03183 | t1 | wavelength_nm=400, color=green, pigment_type=pigment (C.I. Pigment Green 58), sample=Bulk powders (Reference),… | [5] |
| Color filter green pigment PG58 (halogenated zinc ph | 0.2668 | t1 | wavelength_nm=450, color=green, pigment_type=pigment (C.I. Pigment Green 58), sample=Bulk powders (Reference),… | [5] |
| Color filter green pigment PG58 (halogenated zinc ph | 0.88536 | t1 | wavelength_nm=534, color=green, pigment_type=pigment (C.I. Pigment Green 58), sample=Bulk powders (Reference),… | [5] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.026 | t1 | wavelength_nm=410, color=red, pigment_type=pigment, sample=Example 1, pigment_dispersed_particle_size_nm=70, c… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.887 | t1 | wavelength_nm=630, color=red, pigment_type=pigment, sample=Example 1, pigment_dispersed_particle_size_nm=70, c… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.028 | t1 | wavelength_nm=410, color=red, pigment_type=pigment, sample=Example 2, pigment_dispersed_particle_size_nm=77, c… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.876 | t1 | wavelength_nm=630, color=red, pigment_type=pigment, sample=Example 2, pigment_dispersed_particle_size_nm=77, c… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.038 | t1 | wavelength_nm=410, color=red, pigment_type=pigment, sample=Example 3, pigment_dispersed_particle_size_nm=85, c… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.878 | t1 | wavelength_nm=630, color=red, pigment_type=pigment, sample=Example 3, pigment_dispersed_particle_size_nm=85, c… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.022 | t1 | wavelength_nm=410, color=red, pigment_type=pigment, sample=Example 4, pigment_dispersed_particle_size_nm=70, c… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.87 | t1 | wavelength_nm=630, color=red, pigment_type=pigment, sample=Example 4, pigment_dispersed_particle_size_nm=70, c… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.034 | t1 | wavelength_nm=410, color=red, pigment_type=pigment, sample=Example 5, pigment_dispersed_particle_size_nm=78, c… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.874 | t1 | wavelength_nm=630, color=red, pigment_type=pigment, sample=Example 5, pigment_dispersed_particle_size_nm=78, c… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.039 | t1 | wavelength_nm=410, color=red, pigment_type=pigment, sample=Example 6, pigment_dispersed_particle_size_nm=78, c… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.873 | t1 | wavelength_nm=630, color=red, pigment_type=pigment, sample=Example 6, pigment_dispersed_particle_size_nm=78, c… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.024 | t1 | wavelength_nm=410, color=red, pigment_type=pigment, sample=Example 7, pigment_dispersed_particle_size_nm=80, c… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.885 | t1 | wavelength_nm=630, color=red, pigment_type=pigment, sample=Example 7, pigment_dispersed_particle_size_nm=80, c… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.026 | t1 | wavelength_nm=410, color=red, pigment_type=pigment, sample=Example 8, pigment_dispersed_particle_size_nm=90, c… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.883 | t1 | wavelength_nm=630, color=red, pigment_type=pigment, sample=Example 8, pigment_dispersed_particle_size_nm=90, c… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.026 | t1 | wavelength_nm=410, color=red, pigment_type=pigment, sample=Example 9, pigment_dispersed_particle_size_nm=90, c… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.882 | t1 | wavelength_nm=630, color=red, pigment_type=pigment, sample=Example 9, pigment_dispersed_particle_size_nm=90, c… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.026 | t1 | wavelength_nm=410, color=red, pigment_type=pigment, sample=Example 10, pigment_dispersed_particle_size_nm=75, … | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.885 | t1 | wavelength_nm=630, color=red, pigment_type=pigment, sample=Example 10, pigment_dispersed_particle_size_nm=75, … | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.026 | t1 | wavelength_nm=410, color=red, pigment_type=pigment, sample=Example 11, pigment_dispersed_particle_size_nm=80, … | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.883 | t1 | wavelength_nm=630, color=red, pigment_type=pigment, sample=Example 11, pigment_dispersed_particle_size_nm=80, … | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.025 | t1 | wavelength_nm=410, color=red, pigment_type=pigment, sample=Example 12, pigment_dispersed_particle_size_nm=85, … | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.882 | t1 | wavelength_nm=630, color=red, pigment_type=pigment, sample=Example 12, pigment_dispersed_particle_size_nm=85, … | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.025 | t1 | wavelength_nm=410, color=red, pigment_type=pigment, sample=Example 13, pigment_dispersed_particle_size_nm=90, … | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.879 | t1 | wavelength_nm=630, color=red, pigment_type=pigment, sample=Example 13, pigment_dispersed_particle_size_nm=90, … | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.068 | t1 | wavelength_nm=410, color=red, pigment_type=pigment, sample=Comparative Example 1, pigment_dispersed_particle_s… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.052 | t1 | wavelength_nm=410, color=red, pigment_type=pigment, sample=Comparative Example 2, pigment_dispersed_particle_s… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.034 | t1 | wavelength_nm=410, color=red, pigment_type=pigment, sample=Comparative Example 3, pigment_dispersed_particle_s… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.012 | t1 | wavelength_nm=410, color=red, pigment_type=pigment, sample=Comparative Example 4, pigment_dispersed_particle_s… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.016 | t1 | wavelength_nm=410, color=red, pigment_type=pigment, sample=Comparative Example 5, pigment_dispersed_particle_s… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.012 | t1 | wavelength_nm=410, color=red, pigment_type=pigment, sample=Comparative Example 6, pigment_dispersed_particle_s… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.03 | t1 | wavelength_nm=410, color=red, pigment_type=pigment, sample=Comparative Example 7, pigment_dispersed_particle_s… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.017 | t1 | wavelength_nm=410, color=red, pigment_type=pigment, sample=Comparative Example 8, pigment_dispersed_particle_s… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.011 | t1 | wavelength_nm=410, color=red, pigment_type=pigment, sample=Comparative Example 9, pigment_dispersed_particle_s… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.005 | t1 | wavelength_nm=410, color=red, pigment_type=pigment, sample=Comparative Example 10, pigment_dispersed_particle_… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.022 | t1 | wavelength_nm=410, color=red, pigment_type=pigment, sample=Comparative Example 11, pigment_dispersed_particle_… | [6] |
| Color filter red pigment layer (LCD, DPP + anthraqui | 0.022 | t1 | wavelength_nm=410, color=red, pigment_type=pigment, sample=Comparative Example 12, pigment_dispersed_particle_… | [6] |
| Color filter red pigment layer with IR-cut dye (CMOS | 0.1 | t1 | wavelength_nm=400, color=red, thickness_um=1.0, pigment_type=pigment, sample=Example 14 | [4] |
| Color filter red pigment layer with IR-cut dye (CMOS | 0.09 | t1 | wavelength_nm=530, color=red, thickness_um=1.0, pigment_type=pigment, sample=Example 14 | [4] |
| Color filter red pigment layer with IR-cut dye (CMOS | 0.99 | t1 | wavelength_nm=610, color=red, thickness_um=1.0, pigment_type=pigment, sample=Example 14 | [4] |
| Color filter red pigment layer with IR-cut dye (CMOS | 0.51 | t1 | wavelength_nm=910, color=red, thickness_um=1.0, pigment_type=pigment, sample=Example 14 | [4] |
| Color filter red pigment layer with IR-cut dye (CMOS | 0.17 | t1 | wavelength_nm=400, color=red, thickness_um=1.0, pigment_type=pigment, sample=Example 23 | [4] |
| Color filter red pigment layer with IR-cut dye (CMOS | 0.11 | t1 | wavelength_nm=530, color=red, thickness_um=1.0, pigment_type=pigment, sample=Example 23 | [4] |
| Color filter red pigment layer with IR-cut dye (CMOS | 0.7 | t1 | wavelength_nm=610, color=red, thickness_um=1.0, pigment_type=pigment, sample=Example 23 | [4] |
| Color filter red pigment layer with IR-cut dye (CMOS | 0.8 | t1 | wavelength_nm=910, color=red, thickness_um=1.0, pigment_type=pigment, sample=Example 23 | [4] |
| Color filter red pigment layer with IR-cut dye (CMOS | 0.16 | t1 | wavelength_nm=400, color=red, thickness_um=0.9, pigment_type=pigment, sample=Example 24 | [4] |
| Color filter red pigment layer with IR-cut dye (CMOS | 0.11 | t1 | wavelength_nm=530, color=red, thickness_um=0.9, pigment_type=pigment, sample=Example 24 | [4] |
| Color filter red pigment layer with IR-cut dye (CMOS | 0.72 | t1 | wavelength_nm=610, color=red, thickness_um=0.9, pigment_type=pigment, sample=Example 24 | [4] |
| Color filter red pigment layer with IR-cut dye (CMOS | 0.78 | t1 | wavelength_nm=910, color=red, thickness_um=0.9, pigment_type=pigment, sample=Example 24 | [4] |

출처

| # | 제목 | DOI / URL | 종류 |
| --- | --- | --- | --- |
| [1] | A Color Television Camera Using a Single Interline Transfer CCD Image Sensor With Color Filter Array (Morishita, 1981) | DOI 10.1109/tce.1981.273521 | journal |
| [2] | Toyo Ink color filter photoresist technical datasheet | Toyo Ink SC Holdings | datasheet |
| [3] | Investigation and comparison of the influence of modified DBR and yellow color filters for quantum dot color conversion-based micro LED applications | DOI 10.1016/j.heliyon.2024.e35492 | journal |
| [4] | Pigment dispersion liquid containing organic color pigment and infrared absorbing dye, colored resin composition, and optical filter (Nippon Kayaku) U | https://www.freepatentsonline.com/10370464.html | other |
| [5] | Pigment composition for green filter and production method thereof (M. Technique) US11180658B2, Table 3 | https://www.freepatentsonline.com/11180658.html | other |
| [6] | RED COLORING MATTER COMPOSITION AND COLOR FILTER (Toray Industries) JP2006307149A / JP4821316B2, Table 2 | https://patents.google.com/patent/JP2006307149A/en | other |

## 4.5  비가역 전이 — 가역 구간의 시한

### 일중항 산소 수율 Φ_Δ  (1)  —  13건

| 재료 | 값 | 등급 | 조건 | 출처 |
| --- | --- | --- | --- | --- |
| H2TPP free-base porphyrin dye (5,10,15,20-tetrapheny | 0.68 | t1 | matrix=toluene solution (~1e-6 M), wavelength_nm=370, temperature_C=25 | [1] |
| PdOEP red phosphorescent dopant (palladium(II) octae | 0.93 | t1 | matrix=toluene solution (~1e-6 M), wavelength_nm=370, temperature_C=25 | [1] |
| PdTPP red phosphorescent dopant (palladium(II) meso- | 0.9 | t1 | matrix=toluene solution (~1e-6 M), wavelength_nm=370, temperature_C=25 | [1] |
| Pt(BPI-Et)(3-thienylacetylide) red Pt(II) phosphor / | 0.369 | t1 | matrix=toluene solution (1e-5 M), wavelength_nm=480, temperature_K=293 | [2] |
| Pt(BPI-Et)(4-dimethylaminophenylacetylide) red Pt(II | 0.034 | t1 | matrix=toluene solution (1e-5 M), wavelength_nm=480, temperature_K=293 | [2] |
| Pt(BPI-Et)(4-fluorophenylacetylide) red Pt(II) phosp | 0.313 | t1 | matrix=toluene solution (1e-5 M), wavelength_nm=480, temperature_K=293 | [2] |
| Pt(BPI-Et)(4-methoxyphenylacetylide) red Pt(II) phos | 0.212 | t1 | matrix=toluene solution (1e-5 M), wavelength_nm=480, temperature_K=293 | [2] |
| Pt(BPI-Et)(phenylacetylide) red Pt(II) phosphor / TT | 0.73 | t1 | matrix=toluene solution (1e-5 M), wavelength_nm=480, temperature_K=293 | [2] |
| [Pt(L1)(acac)] cyclometalated Pt(II) orange-red phos | 0.38 | t1 | matrix=deaerated dichloromethane (DCM) solution, wavelength_nm=440, temperature_C=25 | [3] |
| [Pt(L2)(acac)] cyclometalated Pt(II) orange-red phos | 0.54 | t1 | matrix=deaerated dichloromethane (DCM) solution, wavelength_nm=440, temperature_C=25 | [3] |
| [Pt(L3)(acac)] cyclometalated Pt(II) orange-red phos | 0.39 | t1 | matrix=deaerated dichloromethane (DCM) solution, wavelength_nm=440, temperature_C=25 | [3] |
| [Pt(L4)(acac)] cyclometalated Pt(II) orange-red phos | 0.3 | t1 | matrix=deaerated dichloromethane (DCM) solution, wavelength_nm=440, temperature_C=25 | [3] |
| [Pt(L5)(acac)] cyclometalated Pt(II) orange-red phos | 0.58 | t1 | matrix=deaerated dichloromethane (DCM) solution, wavelength_nm=440, temperature_C=25 | [3] |

출처

| # | 제목 | DOI / URL | 종류 |
| --- | --- | --- | --- |
| [1] | Banaszek et al., Enhancing Photostability by Thermodynamic and Kinetic Factors: Free-Base and Palladium meso-Aryl-octaethylporphyrins, J. Phys. Chem. | DOI 10.1021/acs.jpcb.5c02423 | journal |
| [2] | Payce et al., Energy Upconversion Using Platinum(II)-BPI Photosensitizers, Inorg. Chem. 64 (2025) 24851-24864, Table 8 ('A Comparison of the Solvent D | DOI 10.1021/acs.inorgchem.5c04677 | journal |
| [3] | Fitzgerald et al., Organometallic Platinum(II) Photosensitisers that Demonstrate Ligand-Modulated Triplet-Triplet Annihilation Energy Upconversion Eff | DOI 10.1002/chem.202203241 | journal |

# 5. 미확보 물성과 조달 경로

## 5.1  1순위 — 절대 시간 스케일을 여는 것

| 필요 | 왜 | 상태 |
| --- | --- | --- |
| 실제 OCA의 O₂ 확산계수 D | 없으면 “몇 개월에 몇 mm”를 못 답한다 | 문헌으로 채울 수 없음 |
| 아크릴레이트 O₂ 용해도 S | 외기 분압 → 막 내부 농도 경계조건 | 문헌으로 채울 수 없음 |

이 둘은 문헌으로 못 채운다. "optically clear adhesive" AND "Barrer" 검색 0건이고 3M OCA 데이터시트에 OTR 항목 자체가 없다. OCA는 배리어 부품이 아니라 업체가 측정·공개할 동기가 없다. 용해도는 원문이 사유를 인쇄한다 — 비극성 영구기체는 극성 고무에서 용해도가 낮아 압력감쇠법 검출한계에 걸린다. 실제로 어느 표에서도 CH₄·CO₂·C₂H₄·C₂H₆는 확산·용해도가 다 채워져 있는데 O₂·N₂·H₂·He만 빈칸이다.

실질적 조달 경로는 셋뿐이다.

| # | 경로 | 비고 |
| --- | --- | --- |
| 1 | Phase 2 데이터로 D_eff 역피팅 | 시험계획이 이미 그렇게 설계돼 있다 — 1순위 |
| 2 | OCA 필름 단품 시편으로 OTR 외주 측정 | §11 업체 요청에 시편 항목이 이미 있다 |
| 3 | 대리계 범위(19 ~ 140 Barrer)로 파라미터 스윕 | 절대값 대신 상하한을 낸다 |

## 5.2  2순위 — 시험 판정의 정밀도

| 필요 | 현황 |
| --- | --- |
| OLED 도판트 계열의 k_q | 지금 2건인데 둘 다 Ir-쿠마린 센서 화합물이고 매질이 CH₂Cl₂ 용액이다. 발광층 고체 매질 값이 필요하다 |
| 박막·고체 매질의 τ₀ | 확보한 73건 대부분이 용액이다. 2.2절이 보여주듯 매질이 소광을 7배 좌우한다 |
| 목표 계열(Ir·Pt OLED 도판트)의 Φ_Δ | 가역 구간의 시한을 정하는 항. 확보한 13건은 포르피린·Pt 착체다 |
| 상용 청색 도판트 τ₀ (DPAVBi·BCzVBi·ADN·TBPe) | OA에 소자 특성표만 있고 용액 광물리 측정이 없다. 지금은 같은 파장대 최신 발광체로 대리한다 |

## 5.3  3순위 — 광경로 정밀화

| 필요 | 현황 |
| --- | --- |
| 적색 CF 380 · 390 nm 투과율 | 0건 — 창의 단파장 쪽 형상을 모른다 |
| 청색 CF 400 nm 실측 | 0건 — 청구항 범위(50~70%)만 있다. 청색이 UV 유입의 가장 큰 문일 가능성이 높다 |
| 녹색 CF 도막의 400 nm | 0건 — 안료 분산액 값만 있다 |
| Irgacure 184 · 651 · 1173의 ε | 0건 — 벤더 PDS가 전부 스펙트럼 그림이고 논문은 정성 서술뿐이다 |

## 5.4  채울 수 없는 것 — 구조적 부재

| 항목 | 이유 |
| --- | --- |
| TFE의 정밀 산소 투과도 | 요구사양(1e-5 cm³/m²/day)이 상용 계측기 하한(약 5e-3) 아래라 업계가 산소는 아예 안 재고 수분(WVTR)만 보고한다. 문헌값이 전부 부등호 표기다 |
| 아크릴 OCA의 산소 실측 | 5.1절 참조 |
| poly(n-butyl acrylate) C3·C4 투과도 | 원표(Mogri & Paul, Polymer 2001)가 유료. 저자 학위논문은 전자 납본 이전이라 리포지토리에 없다 |

# 6. 수집 규율 — 무엇을 걸러냈나

이 과제의 문헌은 값을 그림에만 두는 관행이 특히 강해, 그래프 판독 금지가 가장 크게 작동했다.

| 폐기 사유 | 내용 |
| --- | --- |
| 그래프만 있음 (10건) | 분광·개시제 스펙트럼. 값이 Figure에만 있고 표에 없다 |
| 특허 청구항 범위값 | 설계 상한이지 측정값이 아니다. 다만 실시예 표의 실측은 등록했다 — 이 과제 성과의 상당수가 거기서 나왔다 |
| 문헌 취합표 | Nature Communications의 표준 도판트 14종 τ 표가 매질·분위기 미표기라 통째로 폐기. 2.2절이 보여주듯 매질 없는 τ₀는 60배까지 흔들린다 |
| MD 시뮬레이션 | Kapton 모사 O₂ 투과도가 실측 대비 3000배 어긋났다 |
| 물리적으로 불가능한 표 | PDMS가 N₂ > O₂ > CO₂로 나오는 표. 추출 오류 또는 원문 오식 |
| 검출 하한 부등호 표기 (7건) | “< 1e-3 g/m²/day” 같은 상한 표기는 실측이 아니다 |
| 옆 칸 오독 회피 | K_SV(M⁻¹) 열의 소광종이 O₂가 아니라 TTA-UC 소멸제 DPA였다 |
| 클래스 항목에 값 미부착 | OLED Emitter Layer (Ir phosphor)는 0건을 유지한다. PtOEP 60 µs와 Ir 계열 1~11 µs가 60배 차이라, 클래스에 특정 화합물 값을 붙이면 대표값을 지어내는 것이 된다 |

## 6.1  환산 상수 오류를 수집 배치가 잡았다

작업 지시서에 1 Barrer = 3.348e-19 이라고 적었는데 1000배 틀린 값이다. 정확한 값은 3.3464e-16 mol·m/(m²·s·Pa) 이고 네 방법으로 확증됐다.

| # | 확증 방법 | 결과 |
| --- | --- | --- |
| 1 | 정의에서 직접 유도 | 1e-10 × (1/22414) × 1e-2 / (1e-4 × 1333.2239) = 3.3464e-16 |
| 2 | 카탈로그 기존 실측 역검산 | PET 0.0289 Barrer(문헌 ~0.03), Kapton 0.147(~0.15), PC 0.745(~0.8) |
| 3 | SI·Barrer 병기 문헌 | Membranes 2022, 12, 611 — 4.79e-17 / 1.434e-1 = 3.3427e-16 (0.2% 일치) |
| 4 | 리뷰가 상수를 직접 인쇄 | Macromolecules 2021 — 3.348e-16 |

수집 배치가 지시서를 그대로 믿지 않고 스스로 검산한 덕에 1000배 틀린 값이 대량 유입되지 않았다.